Carbon Paste Electrodes in Modern Electroanalysis

Ivan Švancara,1  Karel Vytřas,1  Jiří Barek,2  Jiří Zima 2

1 Department of Analytical Chemistry, Faculty of Chemical Technology, University of Pardubice, nam. Cs. legii 565, CZ-532 10 Pardubice, Czech Republic; 2 UNESCO Laboratory of Environmental Electrochemistry, Department of Analytical Chemistry, Charles University, Albertov 2030, CZ-128 43  Prague 2, Czech Republic.

Dedicated to the Memory of Professor Jaroslav Heyrovsky

on the Occasion of the 110th Anniversary of His Birth

__________________________________________________________________________

ABSTRACT: Recent trends and advances in the electrochemistry with both unmodified and modified  carbon paste electrodes are reviewed (247 refs). The present day’s knowledge of their basic physico-chemical properties and characteristics is surveyed, including some specifics important in electrochemical measurements. Special attention is paid to the possibilities of carbon paste-based electrodes in electrochemical investigations and in modern electroanalysis of inorganic ions or molecules, organic substances, biologically important compounds, and pharmaceuticals.

KEY WORDS: carbon paste electrodes, electroanalysis, review.

ABBREVIATIONS: ACV, alternating current voltammetry; A(C)SV, anodic (cathodic) stripping voltammetry; ADH, alcohol dehydrogenase; AdSV, adsorptive stripping voltammetry; AMP, amperometry; ASV, anodic stripping voltammetry; 2-BP, 2-butanone peroxide; bpy, bipyridyl; CCSA, constant current stripping analysis; CMCPEs, chemically modified CPE; CNA, chronoamperometry; CNP, chronopotentiometry; CPEs, carbon paste electrodes; CPEEs, carbon paste electroactive electrodes; CP-ISEs, carbon paste ion-selective electrodes; CPyC, cetylpyridinium chloride; CP-UMEs, carbon paste ultramicroelectrodes; CTAB, cetyltrimethylammonium bromide; CV, cyclic voltammetry; DCSV, direct current stripping voltammetry; DME, dropping mercury electrode; DPDTC, diphenyldithiocarbamate; DPA(C)SV, differential pulse anodic (cathodic) stripping voltammetry; EIA, enzyme immunoanalysis; FIA, flow injection analysis; FDH, fructose dehydrogenase; GIDH, glycerol dehydrogenase; GOD, glucose oxidase; HRP, horseradish peroxidase; HTTA, thiophenecarboxylic trifluoroacetone; LADH, lipoamide dehydrogenase; LDH, lactate dehydrogenase;  LOd, lactate oxidase; LSV, linear scan voltammetry; MCPE, modified carbon paste electrode; NPOE, 2-nitrophenyl octyl ether; NMP, N-methylphenazonium; NiTsPc, nickel tetrasulfonated phthalocyanine; Pf, Pseudomonas fluorescens; PAP, poly(o-aminophenol); PEG, polyethylene glykol; PEI, polyethyleneimine; PNA, peptide nucleic acid; POL, polarography; PPD, poly(o-phenylenediamine); PQQ, pyrrolo quinoline quinone; PSA, potentiometric stripping analysis; PVP, poly(4-vinylpyridine); R.S.D., relative standard deviation, Septonex, 1-ethoxycarbonylpentadecyl-trimethylammonium bromide; SPEs, screen printed electrodes; SPPM, spectrophotometry;  ST, titanized silica gel; SWV, square wave voltammetry; TCP, tricresyl phosphate; TEMPO, 2,2,6,6-tetramethylpiperydinyloxy; V, voltammetry.

TABLE OF CONTENTS

##### I.  INTRODUCTION ..................................................................................................

II. CARBON  PASTE  AS  ELECTRODE  MATERIAL   ...........................................

##### A. Unmodified (Bare) Carbon Pastes   .................................................................................

# B. Modified Carbon Pastes   ................................................................................................

III.  SOME TRENDS IN ELECTROCHEMICAL INVESTIGATIONS

WITH CARBON PASTE ELECTRODES   .............................................................

A.  Construction of Carbon Paste Electrodes   .....................................................................

B.  Some Advances in Characterisation of Carbon Pastes   ..................................................

C.  Main Trends in Electrochemical Studies Employing Carbon

Paste Electrodes   ..........................................................................................................

IV.  ELECTROANALYTICAL APPLICATIONS OF UNMODIFIED

AND MODIFIED CARBON PASTE ELECTRODES   ........................................

A.  Inorganic Analysis   .......................................................................................................

B.  Organic  Analysis   .........................................................................................................

References ………………………………………………………………………………

##### I.  INTRODUCTION

In 1958, shortly before Professor Jaroslav Heyrovský received the Nobel Prize for Chemistry and his polarographic method became known worldwide, Adams reported on a new type of electrode.1 The proper material of this sensor was formed by a mixture of carbon powder with a liquid non-electroactive binder and called simply “carbon paste”.  It is interesting to notice that the discovery of carbon paste had closely been connected with Heyrovský’s polarography and his dropping mercury electrode (DME). Several years after the carbon paste had been first introduced, its inventor admitted that his original idea was to develop “dropping carbon electrode”.2 Such a sensor was to be constructed similarly like the DME, i.e., from a reservoir with suspension of carbon powder in a liquid and connected to a capillary, allowing one to obtain periodically renewable droplets of “carbon electrode”. The author hoped that this set-up could serve as a certain analogy to the DME for anodic oxidations of organic compounds where mercury-based electrodes were inapplicable. Although practical experiments with carbon dropping electrode failed, the above-mentioned mixture of carbon powder and a binder prepared in thicker consistency was presented as promising electrode material. Its perspectives were emphasised already in the pioneering report1 and the oncoming boom in the field of electrochemical sensors has confirmed such anticipations.

Carbon paste electrodes (CPEs) and related sensors underwent an attractive development. Its inspiring history, illustrating potentialities of electrochemistry as a whole and revealing numerous connections with the current trends, can be overviewed on some important moments and periods:

 1959-1963: Introduction of Carbon Paste and Its First Applications. The very beginnings of the electrochemistry at CPEs were associated with the research activity of Adams’s group. They postulated first basic characteristics of carbon pastes and some rules for their usage. The initial stage is typical for a rather specialised field of applications; CPEs having been employed mainly in studying the mechanisms of electrode reactions of various organic compounds.3  In that period, reviewed by Adams himself,4 the publications of other authors had appeared only very rarely.

 1964,1965:  First Modifications of Carbon Pastes. The composite nature of carbon pastes and their easy preparation were undoubtedly stimulating factors for altering the properties of originally binary mixtures by another component admixed in. Again, in Adams’s laboratory,3 two such novel carbon pastes had been born. The first type5 containing an organic substance dissolved in the binder and serving to the study the electrode behaviour of the substance itself is considered as a pioneering step in the field of carbon paste electroactive electrodes. The second one6  prepared by rubbing a modifier into the paste had then represented apparently the first case when direct modification of a CPE had resulted in the aimed improving of the electrode performance.

 1974: Appearance of Carbon Pastes with Electrolytic Binder. The replacement of common non-electroactive pasting liquids by electrolyte solutions7 opened the avenue for a specific branch of the electrochemistry of carbon paste electroactive electrodes, allowing one to investigate the redox behaviour as well as various structural and morphological changes of inorganic compounds dissolved directly in the electrolyte. At present, studies of this kind usually belong to a special field of the so-called  solid-state electrochemistry.8

 1981-1990: The Era of Chemically Modified Carbon Pastes. The attempts to utilise favourable mechanical and electrochemical properties of carbon pastes for the preparation of a new generation of sensors culminated at the beginning of the 80s. Modification of a carbon paste by impregnating the carbon particles with methanolic solution of dimethylglyoxime9 represents another milestone in the history of CPEs. It was first attempt when classical analytical reagent had served as selective modifier, thus initiating a very successful role of chemically modified carbon paste electrodes (CMCPEs) in electrochemical analysis as shown in a review covering this period.10 Since that time, the number of publications dealing with chemically modified carbon paste-based electrodes started to grow exponentially and this trend continued over the next decade when other review articles had appeared.11-15

 1988:  Biologically Modified Carbon Pastes as Enzymatic Biosensors. Hand in hand with a rapid development of CMCPEs, favourable mechanical and electrochemical properties of carbon pastes were tested for the preparation of special sensors containing enzymes allowing one to monitor some enzymatically catalysed reactions of biologic substances. The priority in this area can be attributed to Matuszewski and Trojanovicz16 who have reported on a CPE with glucose oxidase blended into the carbon paste. This way of anchoring enzymes to an electrode material immediately attracted biochemists and carbon paste-based enzymatic biosensors had rapidly come to the fore. Retrospectively, they have occupied a very significant position in the family of CPEs when having finally formed a specific independent area similarly like electroactive carbon pastes in the electrochemistry of solids. A comprehensive overview mapping the whole genesis of such biosensors was presented by Gorton,17 some other articles have appeared more recently.18,19

 1991:  Robust Carbon Composites Competing with Carbon Pastes. Probably ultimate significant point in hitherto commented chronology is a starting inclination to replace soft carbon pastes by materials of related character with respect to ease of modifying, but with more robust matrix.20 Such a substrate has proved itself to be convenient for preparation of screen-printed electrodes (SPEs) that co-determine the newest trends in electrochemistry.21

The entire history of the electrochemistry with carbon paste-based electrodes is documented on approx. thousand original papers when about 50-100 publications have arrived annually in the last five years.22 In this article, the recent period of 1995-2000 was summarised with particular interest in order to cover the current trends in the topic since the last comprehensive review papers of similar focus had been published.13,15

II. CARBON  PASTE  AS  ELECTRODE  MATERIAL

##### A. Unmodified Carbon Pastes

Due to a rapid development of various types of modified carbon pastes, it was necessary to introduce a new adequate specification. Classically, all carbon pastes were binary mixtures prepared from carbon powder and organic liquid of non-electrolytic character. Now, such mixtures are classified as bare (“virgin” or, more often, as unmodified carbon pastes.13

For long time, the choice of the main constituents for carbon pastes was rather monotonic and, in fact, there was no reason to seek new alternative materials. The properties of conventional paste mixtures from spectroscopic graphites and paraffin oils were found satisfactory for a majority of applications, including very popular modifications. Nevertheless, also in this area, the recent years have brought some interesting innovations.

The proper electroactive moiety in carbon pastes is still graphite powder with micrometric particles of high purity and distribution uniformity. Such materials are now commonly available on the market as spectroscopic graphites and may be ordered from annual catalogues of renowned distributors such as Aldrich, Sigma, Fluka or Riedel-de-Haen. These products absolutely prevail in the composition of carbon pastes used in the last years. According to the authors’ own experience, especially suitable are “RW-B” or “Sigradur” graphites (ref.13 and refs. therein) offered by factories specialised in production of carbon materials. Usually, graphite powders are not further pre-treated prior to use. Some procedures made in the past and concentrated on lowering undesirable absorption capabilities of some commercial graphites (e.g. 23) seem to be too complicated compared to their benefit. From a present day’s point of view, it is more effective to perform some test experiments with newly made pastes that reveal excessive absorptiveness of some graphites.24 Then, it is better to choose some commercially available powders with specially pre-treated surface exhibiting only negligible absorption capability.25

As non-electrolytic binders, two trademark products of spectroscopic paraffin oils are predominantly used. Nujol (Aldrich) and Uvasol (Merck) figure in Experimental sections of almost all recent papers (13-15,17 and refs. therein). These non-polar pasting liquids fulfil all the important criteria; both are sufficiently chemically inert, insulating, non-volatile, water-immiscible, and forming paste mixtures of fine consistency. However, there also are some less favourable characteristics of pastes made from both oils; for instance, their vulnerability in media with organic solvents.6,11 In this respect, better experience has been gained with silicone oil-based carbon pastes that also represent quite common type of pasting liquid.13,26 Another group of binders are some liquid organophosphates. Although these polar substances had formerly been used as carbon paste modifiers,10,13 their use as binding liquids is relatively new.27 Recent time has brought some interesting applications of these pastes in practical electroanalysis.28-30 Their attractive property is a high ion-pairing ability. However, one has to be aware of their lesser stability and of rather atypical signal-to-noise characteristics requiring special pretreatments.

Numerous practical aspects concerning the preparation of carbon pastes, the choice of suitable components and their ratio, as well as some basic rules of using newly prepared CPEs have been reviewed more recently.26 This review also illustrates that traditional manual procedures of homogenising pastes in a mortar are still preferred despite the fact that ready-to-use carbon paste mixtures are commercially available (e.g. from Metrohm31). Popularity of laboratory preparation of carbon pastes can be explained simply  hand mixing of carbon pastes is advantageous because the analyst can by himself choose the individual components as well as their mutual ratio. This is particularly valid for the preparation of modified carbon pastes.

B. Modified Carbon Pastes

The base of modified carbon pastes is usually a mixture of powdered graphite and non-electrolytic binder.10,13,15 Another constituent in the mixture is then a modifier itself. Modifying agent is usually one substance; but, the pastes can also be modified with two or even more components, which is the case of carbon paste-based biosensors containing enzyme (or its carrier) together with appropriate mediator (ref.17 and refs. therein) or CMCPEs with a mixture of two modifiers.32 The amount of modifier in the paste usually varies between 10-30% (w/w), depending on the character of modifying agent and its capability of forming enough active sites in modified paste (e.g., functional groups immobilised at the electrode surface28 or molecules of an extractant in the bulk 29,30).

In general, the main reason to modify an electrode is to obtain qualitatively new sensor with desired, often pre-defined properties. Regarding this, carbon pastes undoubtedly represent one of the most convenient materials for the preparation of modified electrodes.10 In contrast to relatively complicated modifications of solid substrates, the preparation of CMCPEs is very simple, typically, by means of various alternative procedures. Modifier can be dissolved directly in the binder13,32,33 or admixed mechanically to the paste during its homogenisation.13,34,35 It is also possible to soak graphite particles with a solution of a modifier, and after evaporating the solvent, use so impregnated carbon powder.9,36 Finally, already-prepared pastes can be modified in situ.28 Whereas direct modifications obviously provide special sensors for one-purpose use, considerate in situ approaches offer a possibility to employ the same carbon paste for repetitive modifications with different agents.

Kalcher10 has made a classification of four possible functions of modifiers that can be summarised in this way:

  preferential entrapment of desired species  (e.g. preconcentration in stripping analysis)

  mediation of electrode reactions via immobilised molecules or their fragments

  acting in catalytic phenomena (catalytic electrochemical responses)

  alteration of the surface characteristics of a CPE

When considering these possibilities in combination with the above-mentioned flexibility of carbon pastes, it is not surprising that, in the last decade, a number and a diversity of substances used for the preparation of CMCPEs have grown in a geometric order. Among modifiers recently used, one can find single compounds,34 sophisticated chemical agents,32,37-46 special inorganic materials and matrices,47-62 or living organisms.63-66 Typical modifiers can be divided into several groups.

 Chemical Compounds and Analytical Reagents. Powdered HgO (yellow form) as a modifier was successfully applied as renewable source of mercury film generated at the carbon paste in anodic stripping voltammetry of heavy metals.34 Classical analytical reagents like dimethyl-glyoxime,37 8-hydroxyquinoline,32,38,39 or derivatives of 2-naphthol40,41 have been used as selective modifiers for adsorptive accumulation of selected ions, which is, regarding CPEs, a practice with long tradition.10-15 Some compounds of this type contained in the paste may be slightly soluble in water and, hence, have to be stabilised against “bleeding”  (dissolution) by fixing with an additional adhesion agent.32

 Ion-Exchangers. A group of substances with ion-pairing properties has always held a significant position among CMCPEs.10-15 Recently, cetyltrimethylammonium bromide (CTAB) served again as a reliable modifier to preconcentrate and detect some less common metal species,42-45 whereas chromatographic packing agent “Amberlite IRC-718” can be recommended for speciation analysis.46

 Clay Minerals (Zeolites and Familiar Materials47-57). These substances of both natural and synthetic origin represent a group of hydrated crystalline aluminosilicates that are capable of acting as both ion-exchangers and  “ion-traps” excluding ion species of inappropriate size. Moreover, zeolites51,52 and related materials (e.g., montmorrilonite,48,49,53 or vermicullite47,50) exhibit also adsorption and catalytic capabilities. Thanks to these synergistic effects, zeolites have become apparently the most frequently used modifiers of the last years as documented in Walcarius’s review.67 Carbon pastes with dispersed zeolites (up to 50% w/w) can be employed to study the behaviour of numerous inorganic ions in their natural environment when zeolite-modified CPEs are applicable to their speciation in real samples.

 Humic Substances.55-59 Extremely voluminous molecules of humic acid and humates are also known as very effective ion-exchangers of natural origin. CPEs modified with humates have been shown to be very convenient to detect noble metal ions.

 Silica and Silica-Containing Matrices.60-62 Current possibilities in production of new synthetic pure and grafted silicas are reflected in intensive development of CMCPEs containing these materials. Carbon pastes based on silica with immobilised inorganic films or organic functional groups permit one to carry out selective preconcentration of various species or their detection via catalytic response. Principles and applications of silica-modified electrodes, including carbon paste sensors, were outlined in a review compiled again by Walcarius.68

 Substrates from Living Organisms.63-66 Sometimes, carbon pastes were also selected as convenient electrode material for modifying with biomass (ref.10-15 and refs. therein). Such trends still continue as can be seen on the use of peat moss 63 or algae 64 or, more recently, bacteria 65 and chitin (horny substance forming insect bodies 66).

Carbon paste electroactive electrodes (CPEEs) can also be regarded as a special kind of modified sensors although species contained in the paste do not play role of classical modifiers. The proper paste of CPEEs is formed by graphite particles bounded with a small portion of strong electrolyte (e.g. 2M H2SO4 69 or KOH 70). Newer approaches 35 tend to omit these traditionally used solutions as very aggressive and attacking the substances admixed into the paste prior to the commencement of the electrochemistry as such.8

Finally, even robust (“solid phase”) carbon pastes are more or less related to a family of modified electrodes because they have been also modified. One of the first pastes of this kind was prepared from fenanthrene 71 that was melted, mixed with graphite and this mixture left to harden. Then, after packing in a holder, the paste was modified in situ. Such solid-like pastes represent a transient element between ordinary carbon paste mixtures and composite solid electrodes15 and, as already mentioned, similar matrices seem to be perspective electrode material for screen-printed electrodes designing in the laboratory.

III.  SOME TRENDS IN ELECTROCHEMICAL INVESTIGATIONS

WITH CARBON PASTE ELECTRODES

A.  Construction of Carbon Paste Electrodes

Typically soft carbon pastes have to be packed into suitable electrode bodies. Their construction, of course, depends on the type of electrode (e.g, whether a macro- or a microvariant is to be used) or upon the character of measurement and the overall electrode cell arrangement (batch versus flow systems).

In common experiments, carbon paste electrode holders did not undergo any dramatic development in their functioning and design.13,15 Still, the most popular bodies are various glass-, PVC tubes and Teflon rods whose end-hole can be easily re-filled with a new portion of carbon paste (e.g. 31,35,42-45,71). Also, simple constructions equipped with a piston for extrusion of the paste24,34,51 are frequently employed, including commercially available products from Metrohm.13 For common CPEs, the actual diameter of the end-hole forming the proper carbon paste surface is being chosen from 2 to 10 mm, which is convenient for a majority of electrochemical measurements.2,26 Both above-mentioned construction variants of CPEs for batch measurements allows to utilise fully one of the most valuable property of carbon pastes  easy and quick surface renewal or, in necessary cases, even removal and renewing of a larger portion of the paste. Practically immediate surface renewal can be achieved by wiping some paste off using a wet filter paper. If being performed carefully,24,26 this procedure provides surface reproducibility nearly comparable to that attained by rather time-consuming circle-like polishing of the electrode surface upon a paper pad.53

More interesting designs of CPEs are usually reported in association with carbon paste-based flow cells,72 electrochemical detectors,73 coulometric,74 amperometric75,76 and potentiometric77 sensors, or some sensing devices for special measurements in vivo.78,79 For instance, electrochemical investigations on modulation of the electrode response can be performed with periodically renewed carbon paste by means of a special cell with doubled carbon paste filling.76 Among others, such a design with intimate surface renewal is very effective in analysis of organic and biological materials where the surface of an electrode may readily be poisoned either with matrix constituents or by electrode reaction products.13,72

A carbon paste electrode with unusually large surface diameter of 20 mm was reported to be convenient for coulometric measurements.74 To the authors’ knowledge, this is the largest active surface that has ever been reported for a CPE used in practical measurements. On the contrary, some authors have described single CPEs whose tip could be measured in micrometers.79 These miniaturized sensors had been popular in the eighties, being introduced again by Adams in brain electrochemistry in vivo.80 Their recent applications are only occasional,81-83  which is a fate quite similar to that of carbon paste-based ultramicroelectrodes (CP-UMEs, 84). CP-UMEs designed as a membrane with micrometric pores filled up with a carbon paste were found to exhibit sigmoidal I-E curves typical for microelectrode arrays. In contrast to this, ordinary CPE give rise to normally shaped cyclic voltammograms. This has revealed that whereas CP-UMEs offer an ensemble of isolated carbon active sites thanks to their separation in the membrane pores, the corresponding active sites around carbon particles in the reference carbon paste are merged in one large surface region behaving like that of common solid macroelectrodes.84,85

Today practically forgotten ensembles of CP-UMEs were, however, worth to mention because of their significant contribution to clarifying the behaviour of carbon paste electrodes with insulating binder. Some newer insights into important aspects of the characterisation of CPEs are summarised below.

B.  Some Advances in Characterisation of Carbon Pastes

Physico-Chemical and Electrochemical Properties

The nature and behaviour of common carbon pastes can be portrayed by means of the following physico-chemical characteristics:

  heterogeneity  (composite character)

  lipophility  (hydrophobicity)

  low ohmic resistance  (high conductivity)

  instability in non-aqueous solutions  (disintegration)

  ageing effects  (limited life-time)

These properties are closely connected with a specific microstructure of carbon pastes. Recently, some newly made real images of the carbon paste microstructure have been presented based on scanning electron- and optical microscopic observations.25,31,34,86 The images have confirmed the conclusions of the previous studies (see review25) that carbon pastes represent mixtures with rather unconsolidated structure where the graphite particles are practically covered with a very thin film of the binder. Nevertheless, the individual graphite particles are apparently in some physical contact beneath the binder layer, which may explain a very low ohmic resistance of most carbon pastes (varying in ohms, max. in tens of ohms24-26). Alternative interpretation of their surprisingly high conductivity can be due to a “tunnel effect” similar to that known for semiconductors.87

The hydrophobicity is apparently the most frequently reported property of carbon paste-based electrodes.11-15,17 The lipophilic character of both CPEs and CMCPEs results, among others, in specific reaction kinetics of many electrode reactions of organic redox systems. [Behind their moderated rates is the repelling effect of pasting liquid hindering the access of hydrophilic species involved in the electrode reactions towards the carbon paste surface.13] Reaction kinetics can also be affected by the quality of graphite itself similarly as with related carbon solid electrodes.4  Finally, even the carbon-to-pasting liquid ratio can play a significant role in this respect. Detailed interpretation of these phenomena and its consequences is, however, out of the scope of this article and can be found in the fundamental report from Adams et al 88 or in some newer papers.24,87

Carbon paste mixtures may undergo significant changes in time (“ageing” of CPEs). This feature, in the literature being mentioned only rarely, has been found characteristic for carbon pastes made of some more volatile binders such as organo phosphates.27 Such undesirable behaviour has confirmed logical assumptions that ageing of carbon pastes is associated solely with the properties of the binder. Until now, any similar role of graphite has not yet been reported.

Specifics of Carbon Pastes

Physico-chemical properties of carbon pastes are always mirrored in the overall electrochemical behaviour of CPEs, resulting in some special features and benefits:

  very low background currents  (favourable signal-to-noise ratio),

  individual polarisability  (with variable potential window),

  specific reaction kinetics  (affected by both carbon paste constituents),

  electrode activity at the carbon paste surface as well as  in the carbon paste bulk,

  variability in utilising  various interactions and their synergistic effects at both CPEs and

CMCPEs (electrolysis, catalysis, adsorption, extraction, ion-pairing, and their combination)

  various alternative procedures for pretreating, conditioning and regenerating the electrode

surface and carbon paste itself.

The individual specific features are discussed in all fundamental reviews devoted to carbon paste-based electrodes10-15,17 or dealing exclusively with their characterisation.26,87  Herein, only selected aspects are noticed and commented in more detail.

Processes and Interactions at the Carbon Paste Surface and in the Carbon Paste Bulk

For a majority of substances, the electrode processes connected with mass- and charge transfer at CPEs are usually interpreted as interactions at the interface “binder layergraphite particles solution (electrolyte)”, which applies also to the above-mentioned electrolytic activations. Interactions of this type can be monitored either as both faradayic and non-faradayic current signals in voltammetry, coulometry, and amperometry, or by means of chemical equilibria in potentiometric measurements.13 Some models combine the principles of mass- and charge transfer with specific transport conditions at CPEs. This is the case of so-called “membrane model” assuming extraction (penetration) of some highly lipophilic molecules through the liquid binder layer.89

Electrolytic Phenomena at Carbon Pastes

Polarisation of Bare Carbon Pastes. In voltammetry, the polarisability of carbon pastes was long time believed to depend on the functioning of graphite and the role of pasting liquid was considered as less significant, influencing positively only the background currents level. Recent studies on comparing several CPEs prepared from identical graphite and different liquids have shown that polarisation limits of a CPE can be controlled effectively even via the choice of the binder. For example, tricresyl phosphate-based carbon paste was found to exhibit extreme polarisation limits and could be polarised from -2 to +2 V in an ammonia buffer.27 Such an interval was absolutely unattainable with CPEs from Nujol- and silicone oils and, it is atypically broad for any electrode in aqueous media. A very wide potential window, especially in the negative potential range, was obtained also with a carbon paste containing lipophilic phthalate.27 Thus, it suggests that this property has some general validity and seems to be useful to employ these carbon pastes as the working electrodes for cathodic reductions. For this purpose, paraffin and silicone oil-based CPEs do not offer very good performance and are recommended rather for measurements within the anodic potential range.2,3,11-15  Cathodic polarisations with common CPEs suffer, besides their higher background due to a limited hydrogen overpotential, from the unwanted response of oxygen contained in the paste.2,3,13 Coincidentally, lipophilic esters-containing carbon pastes were found to exhibit – during cathodic polarisation – atypically low signal for oxygen.27 Its lowered content was attributed to a specific carbon paste structure.25 Also this observation has implied a suitability of such pastes for measurements at negative potentials.

Electrolytic Activation. Either anodic and cathodic polarisations performed at extreme potentials or anodic-cathodic cycling are still popular procedures to pretreate the surface of carbon electrodes, including CPEs.90

### In the case of carbon pastes, processes and phenomena associated with activation at positive potentials (anodisation) are mostly interpreted as a partial oxidation of the surface of graphite particles exposed to the solution. During their activation, various oxygen-containing functional groups are formed and instantaneously protonated (see Fig. 1).

Fig. 1	 Anodic activation of the carbon paste surface. A schematic view

Owing to this, these fragments become markedly hydrophilic and repel hydrophobic molecules of the binder. Anodisation thus leads to a removal of lipophilic layer of pasting liquid and results in the principal changes of surface conditions at CPEs. Their surface becomes hydrophilic and behaves, more or less, like that of solid graphites.88  This is of principal importance in organic electrochemistry where the anodisation procedures may significantly improve often unfavourable reaction kinetics at CPEs and remove the undesirable reaction products from the electrode surface. In addition, anodisations can also be a very effective way of enhancing the electrode sensitivity.88,90

### Parent cathodic activations are much less frequent and available literature sources hide only a few notes about their eventual applicability. Despite this, the recent results confirm a high effectiveness of cathodisation; for instance, for suppressing undesirable background currents within the potential range of interest.28,30

An alternative description of the electrochemical reactions at CPEs and their influencing by electrolytic activation is based on a pinhole mechanism.91 The model postulates that the binder layer contains many small pinholes facilitating the charge and mass transfer. Their radius is practically independent of the carbon paste composition; but, may vary in consequence of activation of the carbon paste surface. Some later experiments75,76 showed that applicability of the pinhole mechanism is rather limited and it applies only to some highly hydrophilic species whereas more hydrophobic substances tend to penetrate through the uniform layer of pasting liquid phase according to the above mentioned membrane model.

Electrolytic Preconcentrations at Carbon Pastes. CPEs can also be utilised in stripping analysis for potentiostatic accumulation of selected heavy metals and metalloids. In these cases, it is advantageous to arrange carbon pastes as substrates (supports) plated with either Hg- or Au- films.  At these electrodes, the corresponding metal ions are reduced and deposited in the elemental form either via effective amalgamation with mercury or thanks to the affinity towards gold surface. The proper detection of accumulated species is then carried out by their re-oxidation in anodic voltammetric or potentiometric stripping mode. As documented in a recent review,92 both Hg- and Au-film plated CPEs may provide a performance similar to that of other carbon or metallic electrodes commonly used for electrolytic accumulations  (glassy carbon, mercury drop, platinum or gold disk).

Interactions of Non-Electrolytic Nature

Adsorption, Extraction, Ion-Pairing and Their Combination. Whereas electrolytic processes associated with charge transfer require, in principle, the presence of electroactive sites (i.e., carbon particles), non-electrolytic interactions may proceed  independently on functioning of graphite  in pasting liquid phase or in contact with a special modifying agent.13,87

The role of the binder in non-electrolytic phenomena is rather marginal as far as the  adsorption interactions are concerned. At carbon paste surfaces, adsorption is facilitated mainly via modifiers or by a suitable carbon material.10,13 Carbon pastes as such do not offer any special adsorption capabilities compared to other electrodes.

In contrast to this, extraction of non-polar substances onto the electrode bulk is very typical and even unique property of CPEs if one does not consider some special constructions of membrane sensors.89 Extraction processes at carbon pastes are governed by differences in solubility of extracted species in liquid binder and the respective aqueous phase (supporting electrolyte solution). The resulting distribution ratio then defines the overall effectiveness of extraction that can be controlled via the carbon paste composition, experimental conditions (e.g., pH of the electrolyte and its eventual exchange during measurements) or by chemical structure of the substance itself.13,87

Extractions at CPEs can be combined with adsorption and, more often, with ion-pair formation. Common paraffin- and silicone oil containing carbon pastes possess only very limited ion-pairing capabilities. Several-times mentioned carbon paste mixtures made from tricresyl phosphate (TCP-CPE) are much more convenient. In acidic media, its polar molecules are readily protonated and form ion-associates with various voluminous anions such as

AuCl4- 27 or I- .28-30  These relatively stable ion-aggregates are well extractable onto the TCP-CPE bulk, thus providing a way for their effective accumulation and the subsequent selective detection of the electroactive moiety.27 Regarding CMCPEs, surfactants with long lipophilic chains were repeatedly recommended  as particularly suitable modifying agents for accumulations based on ion-pair formation. Fig. 2 depicts two typical variants of these modifications.

Fig. 2	Carbon paste modified with cationic (a) or anionic (b) surfactant

Cationic surfactant (2a) like cetyltrimethylammonium bromide may thus entrap various anions  such as I- , TiIVO(C2O4)22- or MoO42- 29,42-45) whereas e.g. sodium n-alkyl sullphonate (anionic surfactant, 2b) binds effectively some organic cations31 or Ag+ ions.28 Since both quarternary ammonium salts and alkyl sulphonates are soluble in water, it is necessary to apply in situ modification. The methods utilising both ion-pairing and extraction at carbon paste-based electrodes can purposely be arranged for voltammetric stripping analysis, measurements in flowing streams or for potentiometry (recently as automated titrations15or computerised stripping potentiometry30).

The variability of the processes and interactions at carbon pastes is very useful in both theoretical and applied electrochemistry as they allow performing some special measurements as well as highly selective and sophisticated analytical determinations. Their survey emphasising the recent progress is given in the following sections.

C.  Main Trends in Electrochemical Studies Employing Carbon

Paste Electrodes

As the majority of electrochemical investigations have been carried out with modified carbon pastes, it is quite difficult to comprehend all the advances made recently. Studies with CMCPEs are focused rather individually, depending on the type of modifier, way of modification and its purpose. Nevertheless, main trends of such a research can be illustrated.

Several research groups have achieved a great progress in the area of clay-modified carbon pastes.47-57 Their detailed studies were e.g. dealing with defining the ion-exchanging capacity of various types of zeolite and zeolite-like materials, or mechanisms of ion-exchanging processes for different forms of one species to be analysed. At present, proposed methods are already being successfully applied in practical analysis.67

Numerous investigations were focused on the characterisation of sensors modified with some “fashionable” materials such as fullerenes,93 calixarenes,94 metallothioneins,95 or Ru-(bipyridil)32+-based systems.96 Extensive research work has been done on carbon paste-based biosensors, covering now approx. 50 % of all theoretical studies performed with carbon pastes.22 In this field, a special review can be expected soon.

In solid state electrochemistry with CPEEs,8 various studies on minerals and ores are of continuing interest; for example, pyrite pulps (with traces of Ag and Hg; 97), Egyptian manganese ore,98 galenite99 or sfalerite.100  Defined electrochemical behaviour may sometimes provide information useful for more effective exploitation and technological processing of strategically important ores.

Many attractive applications have resulted from electrochemical investigations of various organic substances such as environmental pollutants, surfactants, food additives, biologically important compounds, or numerous pharmaceutical formulas. The individual methods for their determination are surveyed in Chapter IV.

Finally, some modified carbon pastes can also be chosen as a substrate for rather unusual investigations. For instance, electrochemiluminescent reactions of persulphate in aqueous solutions could be studied with a CPE modified in situ with Ru-compound as catalyser.96 Another CPE with added chlorin-fullerene was capable of producing some photocurrent, thus serving as a novel type of solar cell.93

IV.  ELECTROANALYTICAL APPLICATIONS OF UNMODIFIED

AND MODIFIED CARBON PASTE ELECTRODES

A.  Inorganic Analysis

Table I surveys the applications of both CPEs and CMCPEs in inorganic analysis reported within the period 1995-2000; earlier publications were included only exceptionally (e.g. 124 as hitherto unnoticed in the previous reviews).

The data summarised in Table I underline the individual trends and advances overviewed in the previous text. Among measuring techniques, modern variants of stripping voltammetry have prevailed; mostly, performed with powerful computer-controlled analysers. Their effective combination with carbon paste-based detection systems allows to propose analytical procedures with excellent detection capabilities. The values of detection limits cited in the table have rather informative character; nevertheless, indicate roughly the performance of the corresponding methods. Typically, the detection limits were declared as an estimate for accumulation time varying from 1 to 15 minutes (except 120 min. period reported in 28).

In published determinations, CMCPEs have played a dominant role when representing about 90 % of all applications. Especially those modifications enabling complex reactions with organic reagents (e.g.38-41,116,123) or selective ion-exchange42-45,119-122 were found attractive. Some other methods were based on measurements of electrocatalytical activity.127-131

Application of both CPEs and CMCPEs permit to analyse a wide spectrum of materials of diverse origin: from biological tissues,33,40 via technological and commercial products,43,104,109,128 up to various environmental samples of solid,111 liquid41,118,129 or gaseous111 state. Using carbon paste electrodes, one can analyse either friendly materials like spinach40 or extremely dangerous substance  unstabilised lead azide.124

Quick and inexpensive trace analysis of samples with complex matrix, requiring only minimal pretreatment has been demonstrated using carbon paste electrodes coupled with computer-controlled stripping potentiometry.30,101 So far, this is rather seldom application since stripping potentiometric stations are still preferably equipped with conventional solid electrodes and their employment in inorganic analysis is relatively limited (mostly on determinations of metal ions132,133). Thus, carbon paste electrodes can offer numerous alternative methods, including specific procedures based on synergistic non-electrolytic accumulations or electrocatalytic effects.30,101 Herein, a number of originally voltammetric methods can simply be adapted. And with respect to the fact that, in analysis of real samples, potentiometric stripping analysis is often superior to stripping voltammetry,132,133 one can expect even further improvement of so “novelised” methods.30,136,137 It seems that such an approach may represent one of the future trends in using carbon paste-based electrodes.

It can be concluded that carbon paste electrodes still held a prominent position in modern electroanalysis of inorganic ions and molecules. In particular, the development in the area of CMCPEs have brought a number of new methods and interesting procedures such as speciation analysis with clay-modified carbon pastes for monitoring of heavy metals and their migration in the environment.67  Practically endless number of reagents and materials usable as modifiers in inorganic analysis suggests  that further expansion of various types of CMCPEs can be predicted even at the beginning of a new millennium.

B.  Organic  Analysis

Table II surveys the selected applications of both bare CPEs and CMCPEs use in organic analysis covering the period of last five years. As there are different approaches to compile a representative table for classifying published papers, the type of analyte was chosen as the main classifier. The other classification could be based on already mentioned bare CPEs or anyhow modified CPEs which could be done either by using different modifiers of the carbon paste composition, different mediators of the electron transfer during redox reactions taking place in the solution, enzyme, tissue or cells modifications or immobilization on CPEs, by using redox polymers covering, etc.

Behind the widespread use of carbon pastes in organic analysis several reasons can be identified.  From the chemical point of view, it is mainly the wide freedom in choosing the composition of carbon paste allowing to tailor it for expected analytical use enabling either to highly increase the sensitivity of the determination or simply only to enable it or to suppress the interferences or to establish high selectivity of the determination. Nevertheless, also bare CPEs are still widely used in organic analysis, mainly for direct determination of oxidizable pharmaceuticals in different pharmaceutical formulations or some easily oxidizable phenolics, aromatic amino derivatives or similar compounds. The limit of determination reached by direct analysis on bare CPEs is usually from 1 x 10-6 to 1 x 10-7 M; when accumulation of the analyte on the surface of the working electrode takes place, the limit of determination drops to the concentration of 1 x 10-8 M. By choosing appropriate analyte preconcentration techniques, the limit of determination can further be significantly lowered. This is the case of especially guanine or adenine oxidation based determination of DNA or RNA using potentiometric stripping analysis with adsorptive accumulation where the reported limits of determination are actually at the 10-16 M 174 concentration level for model samples. The same is valid for the analyses of peptides 170, 172 which are usually based on the oxidation of tryptophan, tyrosine or cysteine. Such an extraordinary sensitivity is very promising for example for the construction of disposable senzors for monitoring nucleic acid damage although problems connected with overcoming the interferences signals, lower reproducibility or stability of the signal still persist. The limit of determination for aminoacids in human serum, clinical samples or food samples is much higher, typically around 10-6 to 10-7 M.77, 165 The relatively straightforward use of bare CPEs in organic analysis is justified especially in the field of pharmaceutical analysis for checking the content of drugs in tablets, injections or other formulations where the lower selectivity of electrochemical methods is not so prohibitive due to the strict rules for  the composition of these formulations and the content of the above mentioned specimen. Also the determination of drugs or drug metabolites in urine is well suited for bare CPEs as the matrix is not too complicated and the analyst is usually looking for the presence of a certain substance at appropriate potential interval. Also the products of metabolic drug transformations in human body are often oxidizable allowing to look for either the original drug, or for its metabolite.

The highest number of papers is connected with utilization of different enzymes. From earlier immobilization of enzymes on the surface of carbon pastes, nowadays direct enzyme admixing into the paste is prevalent and quite frequent. Among the enzymes, especially dehydrogenases like lactate dehydrogenase, alcohol dehydrogenase etc., then oxidases like glucose or lactate oxidase and peroxidases like horseradish peroxidase are used most often. Selected applications in Table II illustrate the main trends in this field. In saccharides analysis by far the greatest number of papers deal with determination of glucose, 138-144 mainly in food samples or serum. Although many attempts have been made to decrease the limit of determination of glucose either by choosing different mediators for shuttling the electrons from the reduced form of the enzyme to the electrode,  or by bulk modification of the paste or by immobilization of cells containing glucose oxidase, the lowest reported limit of determination is around 2 x 10-5 M.  The glucose determination is mainly based on glucose oxidase using molecular oxygen as the reoxidation agent in the catalytic cycle with either water or hydrogen peroxide as the final product. The electron transfer mediators vary widely with still no universal mediator for glucose oxidase (see Table II). Very low detection limit of  1.5 pmol is reported for glucose (and urate) in recent paper,144 dealing with peroxidase and ferrocene-embedded CPE with bioelectrocatalytic hydrogen peroxide reduction at 100 mV vs. Ag/AgCl/sat. KCl electrode, where hydrogen peroxide was formed by the action of the corresponding oxidase.  Papers on fructose determination 145,146 report in food analysis the limits od determination around 5 x 10-5 M which are similar to typical previous glucose determinations. Fructose oxidizing enzymes involve either fructose dehydrogenase146 or  pyrrolo quinoline quinone dehydrogenase, 145 the latter not requiring electron transfer mediating.

Another group of organic analytes frequently challenged by CPE are carboxylic acids.147-155 Here lactate is the most frequently studied analyte whose determination is important in food analysis when looking into fermentation processes149,151 or in clinical analysis.150 Simultaneous determination of D- and L-lactate was enabled by D-lactate dehydrogenase coimmobilized with a redox mediator to a polymer backbone and the cofactor NAD(+) and L-lactate oxidase and horseradish peroxidase coadsorbed on graphite. Under flow injection conditions up to 40 samples per hour can be determined although the limits od determination are in the range of (1-10) x 10-5 M.151 The lowest limit of determination of

1 x 10-8  M was reported for ascorbic acid153 in model samples. Methylene green modified CPE153 showed high catalytic activity towards the oxidation of the acid reducing the oxidation overpotential by 400 mV. Again, in practical in vivo measurements the limit of determination for ascorbic acid determination was about 1 x 10-5 M.154  In the group of alcohols156-161 the dominant role plays ethanol which is being determined in different beverages. Although for ethanol the limit of determination of 8 x 10-10 M158 is reported, practical samples show again several orders of magnitude higher limits of determination. The principle of these determinations is mainly connected with electrocatalytic NADH oxidation. When evaluating the papers on amino acids, peptides and hetorocyclic compounds in Table II then it is clear that the best results have been reported on peptides.169-173 The principle of the determination of immunoglobulin G173 is in the attachment of the analyte to a carbon paste with an enzyme label of alkaline phosphatase linked to the antibody. -Naphthol, as the easily oxidizable enzymatic product enabled this extremely sensitive determination with LOD of 2 x 10-12 M and the development of  two immunoelectrochemical devices.

Papers dealing with the determination of either DNA or RNA174-181 almost all show high sensitivity even on bare CPEs and most of the results were obtained using potentiometric stripping analysis following adsorption of the analyte on CPE and origin of the signal is based on guanine oxidation. The CPE pretreatment is also very important and sometimes plays a crucial role.176 In comparison with either DPV or SWV,179 the sensitivity of PSA is higher by several orders of magnitude.174-176,180 It is the high sensitivity of PSA connected with strong adsorption of these analytes on CPE as a preconcentration step which is very promising for future quantitation of nucleic acids and their analogs in diagnostic and biological applications.180 Such a DNA hybridization biosensor has already been constructed181 and it is based on inosine-substituted (guanine free) probe onto the CP transducer where the duplex formation is monitored by the appearance of the guanine oxidation peak of the target.  Quite good reproducibility (R.S.D. of 2 to 3 %) is reported for determination of very low concentrations of nucleic acids178 using flow injection amperometry. Such a very good reproducibility is really quite unusual taking into account the reported picogram quantities and the electrode material used.

The performance of CPEs is quite good  when looking into analyses of pesticides.182-189 The increase in sensitivity was enabled by adsorptive accumulation of the analyte on silica modified CPE182-185 or by formation of host-guest complexes.186-187  These complexes enabled the determination of selected pesticides even in practical samples like soil or natural waters with limits of determination in the concentration range of 10-9 M or even lower.

Phenolics and biogenic amines190-206 are also of continuing interest when working with CPEs. The reported limits of determination based on quinone sensing are quite good (5 x 10-8 M). Copper containing enzyme tyrosinase is used most often for determination of phenols, resulting in formation of ortho-quinone derivatives. The enzymatic activity of tyrosinase towards phenolics enables the determination of different monophenolic compounds but also means low selectivity of tyrosinase based CPE. When properly tailored methods of accumulation are used like biocatalytic accumulation,192 extractive accumulation195 or medium exchange strategy,198 they result in quite low limits of determination even in environmental, clinical or food samples.

The group of pharmaceuticals is very well suited for analysis using CPE.207-224 The reason for it is in quite strict demands on the content of different kinds of pharmaceutical formulations where rarely anything else than the active ingredient is electrochemically active. This is not only the advantage for analysis of pharmaceutical formulations but also for analysis of pharmaceuticals or their metabolites in body fluids, mainly in urine or serum. The most sensitive methods reported were on Clenbuterol,211 Doxazosin,213,214 Imipramine215 and Prazosin221,222 all of them being evaluated on practical biological samples. Clenbuterol determination in bovine serum211 was performed following the accumulation on Nafion-modified CPE when the two-step clean-up procedure included liquid-liquid extraction and solid phase extraction. Tenax-modified CPE enabled the accumulation of Doxazosin213 on the surface of a CPE. 3 min accumulation followed by redissolution technique as DPV and SWV allowed to quantify Doxazosine in very low amounts in human urine.  Sensitive Prazosine determination in urine and formulation is connected with C-8 modification of CPE which allowed more efficient accumulation of the analyte, the final measurements being based on the oxidation of the amine group of Prazosine.

Determination of peroxides225-232 is included mainly for illustration purposes. Although in this case inorganic substance is being determined by CPEs, hydrogen peroxide is the end product of horse radish peroxidase connected methods where the analyte of interest is glucose226, 229,232 or lactate.229

In Table II part dealing with “other substances”, some interesting applications of the use of CPE in organic analysis are summarized. Among them anionic surfactants238 show reasonable limits of determinations, the determination of cocaine235 is quite straightforward with low limit of determination. The determination of growth regulator Roxarsone240 is based on the reduction of the nitro group of the analyte although the determination based on the oxidation of Roxarsone is also possible but less sensitive.

Generally, the possibility of using CPEs for following both oxidation and reduction of organic compounds is also advantageous although, up to now, not fully exploited. This is somewhat surprising when considering a known fact that CPEs offer favourable signal-to-noise characteristics, especially when being polarised anodically. Thanks to very low background currents over the whole anodic range, the bare carbon paste represents one of the most convenient electrode materials for anodic oxidations of organic compounds.4,13 This statement seems to apply also in today’s electrochemistry that is characterised by a myriad of various electrodes and sensors that are being used. The feature of very fine anodic polarisability of CPEs was repeatedly emphasised already during Adams’s era when numerous organic compounds like aromatic amines, phenols or some nitroderivatives had underwent systematic electrochemical investigations (see articles2-4 and refs therein). The results of such studies can be useful also in the present’s day electrochemistry; for instance, as an inspiration in the development of novel methods to determine some organic substances240 and pollutants.184,185

As can be seen from the selected and commented applications of CPEs, their employment in organic electrochemistry offers many diverse possibilities and approaches. Bare carbon pastes are simply usable for the above-commented oxidations and reductions; but, one can also choose them for unique extraction accumulations.220,240 If the surface of a CPE is activated electrolytically,171,179,206 one can aim significant improvements of its kinetic characteristics via lowering the overpotential of some electrode reactions.150,243,156 Special carbon paste mixtures can be operated even in media containing organic solvents.13,26

Such approaches then markedly widen a spectrum of compounds that can be studied using CPEs.

However, analogously to inorganic applications of CPEs, an unflagging optimism is displayed mainly in association with chemically and biologically modified carbon pastes; namely, with a choice of new modifiers, electron transfer mediators and enzymes. Suitably selected modifying agents may catalyse153,159-161 or inhibit134 some reactions.  Modifiers can also participate in some selective accumulations via adsorption182,190 or ion-pairing.246,247 Finally, the use of both CPEs and CMCPEs may result in very sensitive and promising analytical methods173,174 that would show some future trends in applications of carbon paste-based electrodes, including a way of how to move a procedure from model to practical samples.

## ACKNOWLEDGEMENT

## The financial support of the Grant Agency of the Czech Republic (grant no. 203/01/1609) is gratefully acknowledged. J.B. thanks the Czech Ministry of Education, Youth and Sports (research project 113100002) for financial support.

## REFERENCES

1.	Adams, R. N.  Anal. Chem. 1958, 30, 1576.

2.	Adams, R.N.  Electrochemistry at Solid Electrodes.  M. Dekker: New York, 1969.

3.	Wang, J. Electroanalysis. 1999, 11, 283.

4.	Adams, R. N.  Rev. Polarog. (Japan)  1963, 11, 71.

5.	Kuwana, T.; French, W. G. Anal. Chem. 1964, 36, 241.

6.	Marcoux, L.S.; Prater, K.G.; Prater, B.G.; Adams, R.N.  Anal. Chem. 1965, 37, 1446.

7.	Bauer, D.; Gaillochet, M. P. Electrochim. Acta. 1974, 19, 597.

8.	Scholz, F.; Meyer B.  Chem. Soc. Reviews. 1994, 341.

9.	Ravinchandran, K.; Baldwin R. P.  J. Electroanal. Chem. 1981, 126, 293.

10.	Kalcher, K.  Electroanalysis.  1990, 2, 419.

11.	Svancara, I.; Vytras, K.; Renger, F.; Smyth, M. R.  Sb. Ved. Pr., Vys.Sk.

Chemickotechnol., Pardubice.  1992/93, 56, 21.

12.	Ulakhovich, N. A. ; Medyantseva, E. P.; Budnikov, G. K.  Zh. Anal. Khim.

1993, 48, 980.

13.	Kalcher, K.; Kauffmann, J.-M.; Wang, J.; Svancara, I.; Vytras, K.; Neuhold, C.;

Yang, Z.  Electroanalysis. 1995, 7, 5.

14.	Kalcher, K.; Cai, X..-H.; Koelbl, G.; Svancara, I.; Vytras, K.  Sb. Ved. Pr., Vys. Sk.

Chemickotechnol., Pardubice.  1994, 57, 5.

15.	Kalcher, K.; Schachl, K.; Svancara, I.; Vytras, K.; Alemu, H.  Sci. Pap. Univ.

Pardubice, Ser. A  1997, 3, 57.

16.	Matuszewski, W.; Trojanovicz, M.  Analyst. 1988, 113, 735.

17.	Gorton, L.  Electroanalysis.  1995, 7, 23.

18.	Lobo Castanon, M. J.; Alvarez Crespo, S. L.;  Alvarez Gonzalez, M. I.; Saidman,

S.B.; Miranda Ordierez, A.J.; Tunon Blanco, P. Sci. Pap. Univ. Pardubice, Ser. A.

1997, 3, 17.

19.	Pandey, P. C.  Methods Biotechnol. 1998, 6, 81.

20.	Wang, C.; Creasy, K.; Shaw, B.  J. Electroanal. Chem. 1991, 300, 365.

21.	Wang,  J.  Analyst. 1994, 119, 763.

22.	http://wos.isitrial.com/  (2000, December 18)

23.	Lindquist, J.  Anal. Chem. 1973, 45, 1006.

24.	Svancara, I.; Zima J.; Schachl, K. Sci. Pap. Univ. Pardubice, Ser. A.  1998, 4, 49.

25.	Svancara, I.; Hvizdalova, M.; Vytras, K.; Kalcher, K.; Novotny, R. Electroanalysis.

1996, 8, 61.

26.	Svancara, I; Schachl, K. Chem. Listy. 1999, 93, 490.

27.	Svancara, I.; Vytras K.  Anal. Chim. Acta.  1993, 273, 195.

28.	Svancara, I.; Kalcher, K.; Diewald, W.; Vytras, K. Electroanalysis. 1996, 8, 336.

29.	Svancara, I.; Konvalina, J.; Schachl, K.; Kalcher, K.; Vytras, K. Electroanalysis.

1998, 10, 435.

30.	Svancara, I.; Ogorevc, B.; M. Novic, Vytras, K. Talanta. submitted paper.

31.	Digua, K.; Kauffmann, J.-M.; Delplancke, J.-L. Electroanalysis. 1994, 6, 451.

32.	Zhang, Z.-Q.; Liu, H.; Zhang, H.; Li Y.-F. Anal. Chim. Acta. 1996, 333, 119.

33.	Huang, S.-S.; Cheng, Y.-D.; Li, B.-F.;  Liu, G.-D. Mikrochim. Acta. 1998, 130, 97.

34.	Metelka, R.; Vytras, K.; Bobrowski, A.  J. Solid State Electrochem. 2000, 4, 348.

35.	Martinez, R.; Teresa Ramirez, M.; Gonzalez, I.  Electroanalysis. 1998, 10, 336.

36.	Chi, Q. J.; Goepel, W., Ruzgas, T.; Gorton, L.; Heiduschka, P. Electroanalysis.

1997, 9, 357.

37.	Qui, D.-F.; Zhao, Q.; Liu, K.-Z. Huaxue Yanjiu. 1997, 8, 41; cf. Chem. Abstr. 1998, 128, 225285h.

38.	Cai, Q.-T.; Khoo, S. B. Electroanalysis. 1995, 7, 379.

39.	Cai, Q.-T.; Khoo, S. B. Analyst. 1995, 120, 1047.

40.	Khan, M. R. Analyst. 1998, 123, 1351.

41.	Khoo, S. B.; Soh, M.K., Cai, Q.-T.; Khan M. R.; Guo, S.-X.  Electroanalysis.

1997, 9, 45.

42.	Stadlober, M.; Kalcher, K.; Raber, G.; Neuhold, C.  Talanta. 1996, 43, 1915.

43.	Stadlober, M.; Kalcher, K.; Raber, G.  Sci. Pap.Univ. Pardubice, Ser. A.  1997, 3, 103.

44.	Stadlober, M.; Kalcher, K.; Raber, G.  Electroanalysis.  1997, 9, 225.

45.	Stadlober, M.; Kalcher, K.; Raber, G.  Anal. Chim. Acta.  1997, 350, 319.

46.	Viana, M. M. O.; Da Silva, M. P.; Agraz, R.; Procopio, J. R.; Teresa Sevilla, M.;

Hernandez, L. Anal. Chim. Acta. 1999, 382, 179.

47.	Kalcher, K.; Grabec, I.; Raber, G.; Cai, X.-H; Tavcar, G.; Ogorevc, B.

J. Electroanal. Chem. 1995, 386, 149.

48.	Kula, P.; Navratilova, Z.  Fresenius J. Anal. Chem. 1996, 354, 692.

49.	Raber, G.; Kalcher, K.; Stadlober, M.  Sci. Pap.Univ. Pardubice, Ser. A.  1997, 3, 163.

50.	Svegl Grabec, I.; Kolar, M.; Ogorevc, B.; Pihlar, B. Fresenius J. Anal. Chem.

1998, 361, 358.

51.	Walcarius, A.  Anal. Chim. Acta. 1999, 338, 79.

52.	Walcarius, A.; Mariaaulle, P.; Lamberts, L.  J. Electroanal. Chem. 1999, 4653, 100.

53.	Navratilova, Z.; Kula, P.  J. Solid State Electrochem. 2000, 4, 342.

54.	Svegl Grabec, I.; Ogorevc, B. Fresenius J. Anal. Chem. 2000, 367, 701.

55.	Navratilova, Z.; Kula, P. Sci. Pap.Univ. Pardubice, Ser. A.  1997, 3, 195.

56.	Wang, C.-M.; Zhang, H.-l-.; Sun, Y.; Li, H.-L. Anal. Chim. Acta. 1998, 361, 133.

57.	Wang, C.-M.; Li, H.-L. Electroanalysis. 1998, 10, 44.

58.	Sun, Q.-Y.; Wang, C.-M.; Li, L.-X.; Li, H.-L. Fresenius J. Anal. Chem.

1999, 363, 114.

59.	Wang, C.-M.; Zhu, B.; Li, H.-L. Electroanalysis. 1999, 11, 183.

60.	Walcarius, A.; Despas, C.; Trens, P.; Hudson, M. J.; Bessiere, J.

J. Electroanal. Chem. 1998, 453, 249.

61.	Walcarius, A.; Devoy, J.; Bessiere, J.  Environ. Sci. Technol. 1999, 33, 4278.

62.	Walcarius, A.; Luthi, N.;  Blin, J. L.; Su, B. L.; Lamberts, L.

Electrochim. Acta. 1999, 44, 4601.

63.	Yao, H.; Ramelow, G. J. Talanta. 1998, 45, 1139.

64.	Bae, Z.-U.; Kim, Y.-L.; Chang, H.-Y.; Song, F.  Anal. Sci. Technol. 1995, 8, 611.

65.	Hu, R.-Z.; Zhang, W.; Fu, J.-K.; Zhang, W.; Liu Y.-Y.  Anal. Commun. 1999, 36, 147.

66.	Sugawara, K.; Miyasita,T.; Hoshi, S.; Akatsuka, K. Anal. Chim. Acta  1997, 353, 301.

67.	Walcarius, A.  Anal. Chim. Acta. 1999, 384, 1.

68.	Walcarius, A.  Electroanalysis. 1998, 10, 1217.

69.	Ramirez, M. T.; Palomar, M. E., Gonzalez, I.; Rojas-Hernandez, A. Electroanalysis.

1995, 7, 184.

70.	Bezdicka, P.; Grygar T.; Klapste, B.; Vondrak, J.  Electrochim. Acta.  1999, 45, 913.

71.	Diewald, W.; Kalcher, K.; Neuhold, C.; Svancara, I.; Cai, X.-H. Analyst. 1994, 119, 299.

72.	Wang, J.  Anal. Chim. Acta.  1990, 234, 41.

73.	Moeller, A.; Scholz, F. Fresenius J. Anal. Chem. 1996, 356, 160.

74.	Sagar, K.; Fernandez-Alvarez, J. H.; Hua, C.; Munden, R.; Smyth, M. R. Analyst.

1992, 117, 1125.

75. 	Taliene,V.R.; Ruzgas,T.; Razumas,V.; Kulys, J. J. Electroanal. Chem. 1994, 372, 85.

76.	Kulys, J.; Klitgaard, P.; Hansen, H. E.  Mat. Sci. Eng. C, 1996, 4, 39.

77.	Stefan, R.-I.; Van Staden, J. F.; Aboul-Eneim, H. Y.  Anal. Letters. 1998, 31, 1787.

78.	Wang, J.; Hutchins, L.D.; Selim, S.; Cummins, L.B. Biochem. Bioenerg.1984, 12, 193.

79.	O’Neill, R. D.  Analyst. 1994, 119, 767.

80.	Kissinger, P. T.; Hart, J. B.; Adams, R. N.  Brain Res. 1973, 55, 209.

81.	Blaha, C. D.  Pharmacol. Biochem. Behav. 1996, 55, 351.

82.	Kane, D. A.; O’Neill, R. D.  Analyst. 1998, 123, 2899.

83.	Forster, G. L.; Blaha, C. D.  European J. Neurosci. 2000, 12, 3596.

84.	Wang, J.; Zadeii, J. M.  J. Electroanal. Chem. 1988, 249, 339.

85.	Cheng, I. F.; Whiteley, L. D.  Anal. Chem. 1989, 61, 762.

86.	Chadim, P.; Svancara, I.; Pihlar, B.; Vytras, K.  Collect. Chem. Czech. Commun.

2000, 65, 1035.

87.	Svancara, I.; Vytras K. Chemija (Vilnius).  2000, 11, 18.

88.	Rice, M. E.; Galus, Z.; Adams, R. N.  J. Electroanal. Chem. 1983, 143, 89.

89.	Maistrenko, V. N.; Budnikov, G. K.; Gusakov, V. N.  J. Anal. Chem. (Transl.

Zh. Anal. Khim.) 1996, 51, 942.

90. 	Ravinchandran, K.; Baldwin, R. P.  Anal. Chem. 1984, 56, 1744.

91.	Hale, P.D.; Lan, H. L.; Boguslavski, L. I.; Karan, H. I.;  Okamoto Y.; Skotheim, T.A.

Anal. Chim. Acta  1991, 251, 121.

92.	Svancara, I.; Vytras, K.; Kalcher, K. Sci. Pap. Univ. Pardubice, Ser. A.  1997, 3, 207.

93.	Kureishi, Y.; Tamiaki, H.; Shiraishi, H.; Maruyama, K. M.  Biolectrochem. Bioenerg.

1999, 48, 95.

94.	O’Connor, K. M.; Arrigan, D. W. M.; Svehla Gy. Electroanalysis. 1995, 7, 205.

95.	Sestakova, I.; Kopanica, M.; Havran, L.; Paleček, E. Electroanalysis. 2000, 12, 100.

96.	Xu, G.-B.; Dong, S.-J.  Electroanalysis. 2000, 12, 583.

97.	Perdicakis, M.; Grosselin, N.; Bessiere, J.  Anal. Chim. Acta. 1999, 385, 467.

98.	Elsherief, A. E.  Hydrometallurgy. 2000, 55, 311.

99.	Cisneros-González, I.; Oropeza-Guzman, M. T.; Gonzáles I.  Hydrometallurgy.

1999, 53, 133.

100.	Srinivasan, G. N.; Grosselin, N.; Iyer, S. V.  Bull. Electrochem. 2000, 16, 5.

101.	Konvalina, J.; Vytras, K. Electroanalysis. 1998, 10, 787.

102.	Guttmann, M.; Lubert, K. H.; Beyer, L.  Fresenius J. Anal. Chem. 1996, 356, 263.

103.	Schildkraut, D. E.; Dao, P. T.; Twist, J. P.; Davis, A. T.; Robillard, K. A.

Environ. Toxicol. Chem. 1998, 17, 642.

104.	Sugawara, K.; Matsui, H.; Hoshi, S.; Akatsuka, K.  Analyst. 1998, 123, 2013.

105.	Agraz, R.; Teresa Sevilla, M.; Hernández, L.  J. Electroanal. Chem. 1995, 390, 47.

106.	Svancara, I., Matousek, M.; Sikora, E.; Schachl, K.; Kalcher, K.; Vytras, K.

Electroanalysis. 1997, 9, 827.

107.	Won, M.-S.; Kim, H.-J.; Shim, Y.-B.  Bull. Korean Chem. Soc. 1996, 17, 1142;

cf. Chem. Abstr. 1997, 126, 154693k.

108.	Agraz, R.; de Miguel, J.; Teresa Sevilla, M. Electroanalysis. 1996, 8, 565.

109.	Ijeri, V. S.; Srivastava, A. K. Fresenius J. Anal. Chem. 2000, 367, 373.

110.	Ferri, T.; Paci, S.; Morabito, R. Ann. Chim (Rome). 1996, 86, 245.

111.	Shaidarova, L. G.; Ulakhovich, N. A.; Al-Gakhri, M. A.; Budnikov, G. K.;

Glebov, A. N.  J. Anal..Chem. (Transl. Zh. Anal. Khim.). 1995, 50, 692.

112.	Huang, S.-S.; Cheng, Y.-D.; Li, B.-F.; Shi, X.-S.  Fenxi Huaxue. 1998, 14, 126;

cf. Chem. Abstr. 1998, 128, 330507e.

113.	Svancara, I.; Pravda, M.; Hvizdalova, M.; Vytras, K.; Kalcher, K. Electroanalysis.

1994, 6, 663.

114.	Shaidarova, L. G.; Ulakhovich, N. A.; Fedorova, I. L.; Galyametdinov, Yu. G.

J. Anal..Chem. (Transl. Zh. Anal. Khim.). 1996, 51, 687.

115.	Refera, T.; Chandravanshi, B. S.; Alemu, H. Electroanalysis. 1998, 10, 1038.

116.	Wu, J.; Xu W.; Sun, Y. Liuha Jianyan, Huaxue Fence 1995, 31, 157;

cf. Chem. Abstr. 1995, 123, 305311a.

117.	Shumilova, M. A.; Trubachev, A. V.; Kurbatov, D. I.  J. Anal..Chem. (Transl.

Zh. Anal. Khim.) 1997, 52, 753.

118.	Wang, J.; Lu, J.-M.; Larson, D. D.; Olsen, K.  Electroanalysis. 1995, 7, 247.

119.	Lu, G.; Yang, M.; Zhang Q.; Wang, A.; Jin, Z.  Electroanalysis. 1995, 7, 591.

120.	Kwak, M.-K.; Park, D.-S.; Won, M.-S.; Shim, Y.-B. Electroanalysis. 1996, 8, 680.

121.	Svancara, I.; Cermakova, I.; Vytras, K.; Goessler, W.; Kalcher, K. Sci. Pap. Univ.

Pardubice, Ser. A.  1999, 5, 95.

122.	Elmaslout, A.; Benayada, A.; Oudda, H.; Bessiere, J.; Pillet, Y.  Analusis.

1996, 24, 182.

123.	Gomez de Rio, M. I.; de la Fuente, C.; Acuna, J. A.; Vazquez Barbado, M. D.;

Tascon Garcia, M. L.; de Vicente Perez, S.; Sanchez Batanero, P.  Quim Anal.

(Barcelona) 1995, 14, 108.

124.	Razaq Samo, A.; Yar Khahawer, M.; Ali Arbani, S.; Ali Qureshi, G.  J. Chem.

Soc. Pak. 1993, 15, 187.

125.	Neuhold, C. G.; Kalcher, K.; Cai, X.-H.;  Raber, G.  Anal. Letters.  1996, 29, 1685.

126.	Jezkova, J.; Musilova, J.; Vytras, K. Electroanalysis. 1997, 9, 1433.

127.	Cai, X.-H.; Kalcher, K.; Koelbl, G.; Neuhold, C. G.; Diewald, W.; Ogorevc, B.

Electroanalysis. 1995, 7, 340.

128.	Schachl, K.; Alemu, H.; ; Kalcher, K.; Jezkova, J.; Svancara, I.; Vytras, K. Analyst.

1997, 122, 985.

129.	Schachl, K.; Alemu, H.; ; Kalcher, K.; Jezkova, J.; Svancara, I.; Vytras, K. Anal. Letters. 1997, 30, 2655.

130.	Del Campo Santamaria, M.; Vazquez Barbado, M. D.; Tascon Garcia, M. L.;

Sanchez Batanero, P.  Quim. Anal. (Barcelona). 1998, 17, 147.

131.	Cai, X.-H.; Kalcher, K.; Lintschinger, J.; Neuhold, C. G.; Tykarski, J.; Ogorevc, B.

Electroanalysis. 1995, 7, 556.

- Ostapczuk, P. Anal. Chim. Acta. 1993, 273, 35.

- Estela, J.M.; Tomas, C.; Cladera, A.; Cerda, V. Crit. Rev. Anal. Chem. 1995, 25, 91.

- Wang, J.; Chen, L. Anal. Chem. 1995, 67, 3924.

- Perez, E. F.; Neto, G. D.; Tanaka, A. A.; Kubota, L. T. Electroanalysis.  1998, 10, 111.

- Konvalina, J.; Khaled, E.; Vytras, K. Collect. Czech. Chem. Commun. 2000, 65, 1047.

- Svancara, I.; Hocevar, S.B.; Ogorevc, B.; Vytras, K. Electroanalysis. submitted paper.

- Pravda, M.; Adeyoju, O.; Iwuoha, E. I.; Vos, J. G.; Smyth, M. R.; Vytras, K. Electroanalysis.  1995, 7, 619.

- Kawakami, M.; Uriuda, N.; Koya, H.; Gondo, S. Anal. Letters.  1995, 28, 1555.

- Yabuki, S.; Miyutani, F. Biosens. Bioelectron. 1995, 10, 353.

- Kulys, J.; Wang, L.; Hansen, H. E.; Buchrasmussen, T.; Wang, J.; Ozsoz, M. Electroanalysis. 1997, 7, 92.

- Jezkova, J.; Iwuoha, E.I.;  Smyth M. R.; Vytras, K. Electroanalysis. 1997, 9, 978.

- Katrlik, J.; Brandsteter, R.; Svorc, J.; Rosenberg, M.; Miertus, S. Anal. Chim. Acta.  1997, 356, 217.

- Yamamoto, K.; Ohgaru, T.; Torimura, M.; Kinoshita, H.; Kano, K.; Ikeda, T. Anal. Chim. Acta.  2000, 406, 201.

- Parellada, J.; Dominguez, E.; Fernandez, V. M. Anal. Chim. Acta. 1996, 330, 71.

- Paredes, P. A.; Parellada, J.; Fernandez, V. M.; Katakis, I.; Dominguez, E. Biosens. Bioelectron. 1997, 12, 1233.

- Mizutani, F.; Yabuki, S.; Iijima, S. Electroanalysis.  1995, 7, 706.

- Wang, J.; Chen, Q.; Pedrero, M. Anal. Chim. Acta.  1995, 304, 41.

- Spohn, U.; Narasaiah, D.; Gorton, L.; Pfeiffer, D. Anal. Chim. Acta. 1996, 319, 79.

- Colon, C. M.; Guadalupe, A. R. Electroanalysis. 1998, 10, 621.

- Narasaiah, D.; Spohn, U.; Gorton, L. Anal. Letters. 1996, 29, 181.

- Hu, X. Y.; Leng, Z. Z. Anal. Letters. 1995, 28, 2263.

- Yu, A. M.; He, C. X.; Zhou, J.; Chen, H. Y. Fresenius J. Anal. Chem. 1997, 357, 84.

- Lowry, J. P.; Boutelle, M. G.; Oneill, R. D.; Fillenz, M. Analyst. 1996, 121, 761.

- Cai, X.-H.; Ogorevc, B.; Tavcar, G.; Kalcher, K. Electroanalysis. 1995, 7, 639.

- Lobo, M. J.; Miranda, A. J.; Tunon, P.; Electroanalysis. 1996, 8, 591.

- Vijayakumar, A. R.; Csoregi, E.; Heller, A.; Gorton, L. Anal. Chim. Acta. 1996, 327, 223.

- Lobo, M. J.; Miranda, A. J.; Lopez Fonseca, J. M.;  Tunon, P. Anal. Chim. Acta. 1996, 325, 33.

- Alvarez-Gonzales, M. I.; Saidman, S. A.; Lobo-Castanon, M. J.; Miranda-Ordieres, A. J.; Tunon-Blanco, P. Anal. Chem. 2000, 72, 520.

- Malinauskas, A.; Ruzgas, T.; Gorton, L.; Kubota, L. T. Electroanalysis. 2000, 12, 194.

- Chen, H. Y.; Yu, A. M.; Han, J. L.;  Mi, Y. Z. Anal. Letters. 1995, 28, 1579.

- Wang, H. S.; Cui, H.; Zhang, A. M.; Liu, R. M. Anal. Commun. 1996, 33, 275.

- Miland, E.; Ordieres, A. J. M.; Blanco, P. T.; Smyth, M. R.; Fagain, C. O. Talanta. 1996, 43, 785.

- Zen, J. M.; Chen, Y. J.; Hsu, C. T.; Ting, Y. S. Electroanalysis. 1997, 9, 1009.

- Huang, T.; Warsinke, A.; Kuwana, T.; Scheller, F. W. Anal. Chem. 1998, 70, 991.

- Shaidarova, L. G.; Fedorova, I. L.; Ulakhovich, N. A., Budnikov, G. K. J. Anal. Chem. (Transl. Zh. Anal. Khim.).  1997, 52, 238.

- Nalini, B.; Narayanan, S. S. Electroanalysis. 1998, 10, 779.

- Perez, E. F.; Kubota, L. T.; Tanaka, A. A.; Neto, G. D. Electrochim. Acta. 1998, 43, 1665.

- Tomschik, M.; Havran, L.; Fojta, M.; Palecek, E. Electroanalysis. 1998, 10, 403.

- Fernandez-Sanchez, C.; Gonzales-Garcia, M. T.; Costa-Garcia, A. Biosens. Bioelectron. 2000, 14, 917.

- Wang, J.; Rivas, G.; Cai, X.-H.; Chicharro, M.; Farias P. A. M.;  Palecek, E. Electroanalysis. 1996, 8, 902.

- Cai, X.-H.; Rivas, G.; Farias P. A. M.; Shiraishi, H.; Wang, J.;  Palecek, E. Anal. Chim. Acta. 1996, 332, 49.

- Fernandez-Sanchez, C.; Costa-Garcia, A. Biosens. Bioelectron. 1997, 12, 403.

- Wang, J.; Cai, X.-H.; Wang, J. Y.; Jonsson, C.; Palecek, E. Anal. Chem. 1995, 67, 4065.

- Cai, X.-H.; Rivas, G.; Farias P. A. M.; Shiraishi, H.; Wang, J.; Fojta, M.; Palecek, E.  Biosens. Bioelectron. 1996, 40, 41.

- Cai, X.-H.; Rivas, G.; Farias P. A. M.; Shiraishi, H.; Wang, J.;  Palecek, E. Electroanalysis. 1996, 8, 753.

- Wang, J.; Cai, X.-H.; Rivas, G.; Shiraishi, H.; Farias P. A. M.; Dontha, N. Anal. Chem. 1996, 68, 2629.

- Wang, J.; Chen, L.; Chicharro, M. Anal. Chim. Acta.  1996, 319, 347.

- Cai, X.-H.; Ogorevc, B.; Kalcher, K. Electroanalysis. 1995, 7, 1126.

- Wang, J.; Rivas, G.; Cai, X. H.; Chicharro, M.; Dontha, N.; Luo, D. B.; Palecek, E.; Nielsen P. E. Electroanalysis. 1997, 9, 120.

- Wang, J.; Rivas, G.; Fernandes J. R.; Paz, J. L. L.; Jiang, M.; Waymire, R. Anal. Chim. Acta. 1998, 375, 197.

- Fernandez, C.; Reviejo, A. J.; Pingarron, J. M. Analusis. 1995, 23, 319.

- Faller, C.; Meyer, A.; Henze, G. Fresenius J. Anal. Chem. 1996, 356, 279.

- Arranz, A.; deBetono, S. F.; Moreda, J. M.; Cid, A.; Arranz, J. F. Mikrochim. Acta. 1997, 127, 273.

- Arranz, A.; Villalba, M. F.; deBetono, S. F.; Moreda, J. M.; Arranz, J. F. Fresenius J. Anal. Chem. 1997, 357, 768.

- Ulakhovich, N. A.; Priimak, E. V.; Medyantseva, E. P.; Anisimova, L.A.; Al-Gahri, M. A. J. Anal. Chem. (Transl. Zh. Anal. Khim.). 1998, 53, 147.

- Shaidarova, L. G.; Fedorova, I. L.; Ulakhovich, N. A.; Budnikov, G. K. . J. Anal. Chem. (Transl. Zh. Anal. Khim.). 1998, 53, 52.

- Bordes, A. L.; Limoges, B.; Brossier, P.; Degrand, C. Anal. Chim. Acta. 1997, 356, 195.

- Bordes, A. L.; Schollhorn, B.; Limoges, B.; Degrand, C. Appl. Organomet. Chem. 1998, 12, 59.

- Wang, L. H. Analyst. 1995, 120, 2241.

- Burestedt, E.; Emneus, J.; Gorton, L.; Marko Varga, G.; Dominguez, E.; Ortega, F.; Narvaez, A.; Irth, H.; Lutz, M.; Puig, D.; Barcelo, O. D. Chromatogaphia. 1995, 41, 207.

- Wang, J.; Chen, Q. Electroanalysis. 1995, 7, 746.

- Ruzgas, T.; Emneus, J.; Gorton, L.; Marko Varga, G. Anal. Chim. Acta. 1995, 311, 245.

- Wang, H. S.; Zhang, A. M., Cui, H.; Liu, D. J.; Liu, R. M. Microchem. J. 1998, 59, 448.

- Wang, J.; Lu, F.; Kane, S. A.; Choi, Y. K.; Smyth M. R.; Rogers, K. Electroanalysis. 1997, 9, 1102.

- Zoulis, N. E.; Efstathiou, C. E. Anal. Chim. Acta. 1996, 320, 255.

- Castanon, M. J. L.; Ordieres, A. J. M.; Blanco, P. T. Biosens. Bioelectron. 1997, 347, 271.

- Volikakis, G. J.; Efstathiou, C. E. Talanta. 2000, 51, 775.

- Rodriguez, I. N.; Leyva, J. A. M.; de Cisneros, J. L. H. H. Anal. Chim. Acta. 1997, 344, 167.

- Rodriguez, I. N.; Leyva, J. A. M.; de Cisneros, J. L. H. H. Analyst. 1997, 122, 601.

- Cordero-Rando, M. D. M.;  Naranjo-Rodriguez, I.; de Cisneros, J. L. H. H. Anal. Chim. Acta. 1998, 370, 231.

- Yang, Z. P.; Li, Y. B.; Balagtas, C.; Slavik, M.; Paul, D. Electroanalysis. 1998, 10, 913.

- Vanickova, M.; Labuda, J.; Buckova, M.; Surugiu, I.; Mecklenburg, M.; Danielsson, B. Coll. Czech. Chem. Commun. 2000, 65, 1055.

- Foryani, E. S.; Rivas, G. A.; Solis, V. M. J. Electroanal. Chem. 1995, 382, 33.

- Petit, C.; Gonzales-Cortes, A.; Kauffmann, J.-M. Talanta. 1995, 42, 1783.

- Zen, J. M.; Chen, P. J. Anal. Chem. 1997, 69, 5087.

- ElMaali, N. A.; Ghandour, M. A.; Kauffmann, J.-M.  Bioelectroch. Bioener. 1995, 38, 91.

- Posac, J. R.; Vazquez, M. D.; Tascon, M. L.; Acuna, J. A.; de la Fuente, C.; Sanchez-Batanero, P. Talanta. 1995, 42, 293.

- Perlado, J. C.; Zapardiel, A.; Bermejo, E.; Perez, J. A.; Hernandez, L. Anal. Chim. Acta. 1995, 305, 83.

- Wang, J.; Rivas, G.; Cai, X.-H.; Shiraishi, H.; Farias, P. A. M.; Dontha, N.; Luo, D. B.  Anal. Chim. Acta. 1996, 332, 139.

- Moane, S.; Smyth, M. R.; Okeeffe, M. Analyst. 1996, 121, 779.

- Rapicault, S.; Limoges, B.; Degrand, C. Anal. Chem. 1996, 68, 930.

- Arranz, A.; de Betono, S. F.;  Moreda, J. M.; Cid, A.; Arranz, J. F.  Analyst. 1997, 122, 849.

- Arranz, A.; Moreda, J. M.; Arranz, J. F. Mikrochim. Acta. 2000, 134, 69.

- Khodari, M.; Mansour, H.; ElDin, H. S. Anal. Letters. 1997, 30, 1909.

- Ferancova, A.; Korgova, E.; Miko, R.; Labuda, J. J. Electroanal. Chem. 2000, 492, 74.

- Wang, J.; Ozsos, M.; Cai, X.-H.; Rivas, G.; Shiraishi, H.; Grant, D. H.; Chicharro, M.; Fernandes, J.; Palecek, E. Bioelectroch. Bioener. 1998, 45, 33.

- Buchberger, W.; Niessner, G.; Bakry, R. Fresenius J. Anal. Chem. 1998, 362, 205.

- El-Maali, N. A. Bioelectroch. Bioener. 1998, 45, 281.

- Radi, A. Electroanalysis. 1998, 10, 103.

- Arranz, A.; de Betono, S. F.; Echevarria, C.; Moreda, J. M.;  Cid, A.; Valentin, J. F. A. J. Pharm. Biomed. Anal. 1999, 21, 797.

- Arranz, A.; Moreda, J. M.; Arranz, J. F. Quim. Anal. 2000, 19, 31.

- Garcia-Fernandez, M. A.; Fernandez-Abedul, M. T.; Costa-Garcia, A.  Electroanalysis. 2000, 12, 483.

- Vanickova, M.; Buckova, M.; Labuda, J. Chem. Anal. (Warsaw).  2000, 45, 125.

- Oungpipat, W.; Alexander, P. W.; Southwellkeely, P. Anal. Chim. Acta. 1995, 309, 35.

- Li, J.; Tan, S. N.; Ge, H. L. Anal. Chim. Acta.  1996, 335, 137.

- Popescu, I. C.; Csoregi, E.; Gorton, L. Electroanalysis. 1996, 8, 1014.

- Limoges, B.; Degrand C. J. Electroanal. Chem. 1997, 422, 7.

- Liu, H. Y.; Zhang, Z. N.; Fan, Y. B.; Dai, M.; Zhang, X. L.; Wei, J. J.; Qui, Z. N.; Li, H. B.; Wu, X. X.; Deng, J. Q.; Qi, D. Y. Fresenius J. Anal. Chem. 1997, 357, 297.

- Vieira, I. D.; Fatibello, O. Analyst.  1998, 123, 1809.

- Garcia, M. A. V.; Blanco, P. T.; Ivaska, A. Electrochim. Acta.  1998, 43, 3533.

- Compagnone, D.; Schweicher, P.; Kauffman, J.-M.; Guilbault, G. G. Anal. Letters.  1998, 31, 1107.

- Hu, S. S.; Guo, M. D.; Hu, G. Z., Jiang, M. Anal. Letters.  1995, 28, 1993.

- Chicharro, M.; Zapardiel, A.; Bermejo, E.; Perez-Lopez, J. A.; Hernandez, L. Analusis.  1995, 23, 131.

- Fernandez-Abedul, M. T.; Costa-Garcia, A. Anal. Chim. Acta. 1996, 328, 67.

- Charpentier, L.; ElMurr, N. Anal. Chim. Acta. 1995, 318, 89.

- Takayama, K.; Ikeda, T.; Nagasawa, T. Electroanalysis. 1996, 8, 765.

- Hattori, T.; Kato, M.; Tanaka, S.; Hara, M. Electroanalysis.  1997, 9, 722.

- Kinoshita, H.; Torimura, M.; Kano, K.; Ikeda, T. Electroanalysis.  1997, 9, 1234.

- Ahamad, R.; Barek, J.; Rahim Yusoff, A.; Sinaga, S. M.; Zima, J. Electroanalysis. 2000, 12, 1220.

- Kinoshita, H.; Torimura, M.; Yamamoto, K.; Kano, K.; Ikeda, T. J. Electroanal. Chem. 2000, 478, 33.

- Komersova, A.; Bartos, M.; Kalcher, K.; Vytras, K.:  J. Pharm. Biomed. Anal. 1998, 16, 1373.

- Schachl, K.; Alemu, H.; Kalcher, K.; Jezkova, J.; Svancara, I. Sci. Pap. Univ. Pardubice, Ser. A. 1997, 3, 41.

- Novakova M.; Kalcher, K.; Schachl, K.; Komersova A.; Bartos, M.; Vytras, K.  Sci. Pap. Univ. Pardubice, Ser. A. 1997, 3, 139.

- Pravda, M.; Petit, C.; Michotte, Y.; Kauffmann, J.-M.; Vytras K. J. Chromatogr. A. 1996, 727, 47.

- Vytras, K.; Kalous, J.; Jezkova, J.  Egypt. J. Anal. Chem. 1997, 6, 107.

- Vytras, K.; Jezkova, J.; Dlabka, V.; Kalous, J.  Sci. Pap. Univ. Pardubice, Ser. A. 1997, 3, 307.

Table I 	Selected applications of carbon paste electrodes in inorganic analysis

| Analyte | Type of carbon paste electrode (modifier) | Principle(s) of the method |  | Measuring technique (specification) | Detection limit [ sample ] | Cit. |
| --- | --- | --- | --- | --- | --- | --- |
| AuIII | CMCPE (humic acid + ethylendiamine) | ion-pair formation |  | CV, DPSV | 1  10-8 M [model solutions] | 56 |
|  | CMCPE (bacteria) | interaction at electrolytically pretreated surface |  | CSV |  | 65 |
|  | CPE (containing TCP) | ion-pair formation combined with extraction |  | CCSA |  | 101 |
| AgI | CMCPE (containing TCP and modified by heptyl sulfonic acid in situ) | ion-pair formation at cathodically pretreated surface |  | DPASV | 3  10-12 M [tap water] | 28 |
|  | CMCPE (N-benzoyl-N’,N‘-diisobutylthiourea | complex formation followed by reaction with the surface groups |  | DPSV (open circuit) | 1  10-7 M [model solutions] | 102 |
|  | CPE (unmodified) | electrolytic preconcentration |  | SWASV | 2 x 10-7 M [lake and river water] | 103 |
|  | CMCPE (keratin) | accumulation via reaction with functional groups |  | DPCSV | 2  10-8 M [photographic developer] | 104 |
| HgI, HgII | CMCPE (thiolic resin) | complex formation; controlled potential differentiation between both oxidation states |  |  | 2-4 g/L [aquatic samples] | 105 |
|  | CMCPE (humic acid + immobilised functional groups) | accumulation via reaction with -NH2 functional group |  | LSSV | 5  10-8 M [model solutions] | 57 |
| HgII | CPE (plated with Au-film in situ) | electrolytic preconcentration via affinity towards gold |  | DPASV | 3  10-10 M [polluted tap water] | 106 |
|  | CMCPE (vermiculite) | ion-pair formation |  | SWASV | 6  10-8 M [model solutions] | 50 |
| Table I continued |  |  |  |  |  |  |
| CuI | CMCPE (rubeanic acid) | complex formation |  | DPCSV (open circuit) | 8  10-5 M [reference material] | 107 |
| CuI, CuII | CMCPE) (Chelite P) | accumulation via reaction with -NH2 functional group | DPSV |  | 2 x 10-6 M [river water] | 108 |
|  | CMCPE (alga Anabaena + Nafion film) | bioaccumulation effect | DPASV (open circuit) |  | 8  10-5 M [model solutions] | 64 |
|  | CMCPE (crown-ethers) | complexing + ion-exclusion effect | DPCSV |  | 0.050 ppm [alcoholic beverages] | 109 |
| AsIII, AsV | CPE (plated with Au-film in situ) | electrolytic preconcentration onto gold film; reduction intermediate step | DPASV |  | 1 g/L [spiked tap water] | 86 |
| BiIII | CMCPE (Bismuthol II) | accumulation via reaction with –SH functional group | LSCSV (open circuit) |  | 2  10-8 M [model solutions] | 110 |
| PbII | CMCPE (crown-ethers) | complexing + ion-exclusion effect | CSV |  | 3  10-9 M [soil, plants, water, air] | 111 |
|  | CMCPE (tributylphoshate + modification with pyrazolone derivative in situ) | complex formation | DPCSV |  | 1  10-9 M [water, alloy] | 112 |
| CdII | CMCPE (tributylphoshate + modification with pyrazolone derivative in situ) | complex formation | DPCSV |  | 5  10-8 M [waste water, human hair] | 33 |
| ZnII | CPE (containing TCP; plated with Hg-film in situ) | electrolytic preconcentration via amalgamation on mercury film | DPASV |  | 1  10-7 M [tap waters] | 113 |
| Table I continued |  |  |  |  |  |  |
| TlI, TlIII | CMCPE (8-hydroxyquinoline + glycerin) | electrolytic preconcentration; masking with EDTA | DPASV |  | 5  10-9 M [model solutions] | 38,39 |
| FeIII | CPE (unmodified) | electrolytic reduction | DPCSV |  | 1ppm [solid 5-aminoisophthalic acid] | 242 |
| NiII (+ CoII) | CMCPE (aza-crown-ethers) | complexing + ion-exclusion effect | DPCSV (simultaneous d.) |  | 4  10-8 M [model solutions] | 114 |
| CoII | CMCPE (N-p-chlorofenylcinnamo- hydroxamic acid) | complex formation | DPASV |  | 3  10-7 M [vitamin] | 115 |
|  | CMCPE [1-(2-pyridyl-azo)-2-naphthol] |  | DPCSV |  | 6  10-9 M [human hair, liver, spinach] | 40 |
| MnII | CMCPE [1-(2-pyridyl-azo)-2-naphthol] | complex formation | DPCSV (open circuit) |  | 7  10-9 M [sea water] | 41 |
| ZrIV | CMCPE (1-nitroso-2-naphthol) | complex formation equilibrium | potentiometry |  | 1  10-6 M [ceramic glass] | 116 |
| TiIV | CMCPE (CTAB in situ) | ion-pair formation, micellar congregation; reduction intermediate step | DPASV |  | 0.1 g/L [mineral (stone-wool), building material] | 42,43 |
| VV | CMCPE (CTAB; oxalate, in situ) | ion-pair formation, micellar congregation; reduction intermediate step | DPASV |  | 0.07 g/L [alloys] | 43,44 |
| MoVI | CMCPE (CTAB; oxalate, in situ) | ion-pair formation, micellar congregation; reduction intermediate step | DPASV |  | 0.04 g/L [alloys] | 43,45 |
|  | CMCPE (chitin) | electrostatic interaction with functional groups of modifier; medium exchange | ASV |  | 1  10-7 M [sea water] | 66 |
| Table I continued |  |  |  |  |  |  |
| WVI | CMCPE (8-mercaptoquinoline) | complex formation | ASV |  | 1 g/L [model solutions] | 117 |
| UVI | CMCPE (propyl gallate) | complex formation | DPV (field analysis) |  | 1 g/L [ground water] | 118 |
| PdII | CMCPE (dimethylglyoxim) | complex formation | FIA |  | 5  10-7 M [model solutions] | 37 |
|  | CMCPE (sodium humate) | ion-pair formation | LSASV |  | 5  10-7 M [environmental samples] | 58 |
| I- | CMCPE (CTAB in situ) | ion-pair formation | DPSV |  | 0.03 mg/L [table salts] | 119 |
|  | CMCPE (cinchonine) |  |  |  | 8  10-8 M [disifectant] | 120 |
|  | CPE (containing TCP) | ion-pair formation, extraction (cathodisation pretreatment 30) | DPCSV, CCSA |  | 1-3  10-7 M [iodinated and natural table salts] | 29,30 |
|  | CMCPE (Septonex in situ) | ion-pair formation combined with extraction | DPCSV |  | 2  10-7 M [mineral waters] | 121 |
| HPO42- | CMCPE (Hg2HPO4-) | ion-exchange equilibrium | potentiometry |  | - - [conc. phosphoric acid] | 122 |
| NO2- | CMCPE (Prussian Blue) | electrocatalytic effect | LSV |  | 200 ppb [waste water] | 123 |
| N3- | CPE (unmodified) | electrolytic oxidation | LSV (combined with POL at DME) |  | 50 g/m3 [air, lead azide (with or without dextrin)] | 124 |
| Table I continued |  |  |  |  |  |  |
| ClO4- | CMCPE (Amberlite LA2 - admixed; TlIIICl4- in situ) | ion-exchange; catalytic effect | DPV (open circuit) |  | 50 g/L [spiked tap water] | 125 |
|  | CP-ISEs (containing TCP) | ion-pairing with counter-ion (CPyC as titrant) | potentiometry |  | 0.4-2..5  10-6 M [explosives, rocket propellant extracts] | 126 |
| H2O2 | CMCPE (Pd-powder) | electrocatalytic activity | LSV |  | 50 g/L [model solutions] | 127 |
|  | CMCPE (MnO2 as bulk- and film modifier) |  | FIA |  | 45 g/L [hair blonding booster, mouth wash; rainwater] | 128, 129,243 |
|  | CMCPE (MeII-phthalocyanines) |  | CV, DPV |  | 22 ppb [model solutions] | 130 |
| NH2OH | CMCPE (Pd-powder) | electrocatalytic activity | FIA |  | 20 pg [river water] | 131 |
| N2H4 | (immobilized tyrosinase) | inhibition of immobilized tyrosinase | AMP |  | ~ 10-6 M [river, drinking water] | 134 |
|  | (ST-NiTsPc) [mineral oil] | electrocatalytical N2H4 oxidation | CV |  | 1 x 10-5 M [model samples] | 135 |

Table II 	Selected Applications of Carbon Paste Electrodes in Organic Analysis

| Analyte | Type of electrode (modifier) [liquid binder] | Principle(s) of the method | Measuring technique | Detection limit [sample] | Ref. |
| --- | --- | --- | --- | --- | --- |
| # Saccharides |  |  |  |  |  |
| Glucose | (GOD , Os polymer mediator) | Os2+/Os3+ redox mediating | AMP | 2 x 10-3 M [model samples] | 138 |
|  | (GOD , ubiquinone mediator) [paraffin oil] | ubiquinone e- transfer mediating | AMP | 2 x 10-4 M [model samples] | 139 |
|  | (GOD, HRP, 1,1´-dimethylferrocene) [PEG] | reductive current measurement, bienzyme electrode | AMP | 2 x 10-5 M [drinks] | 140 |
|  | (GOD, methylene green) | anodic current measurement | FIA, AMP | ~ 3 x 10-3 M [serum] | 141 |
|  | (GOD, PEI and Os polymer) | Os2+/Os3+ redox mediating | CV, AMP | 2 x 10-3 M [senzor stabilization study] | 142 |
|  | (Aspergillus niger cells cont. GOD and ferrocene) [paraffin oil] | glucose oxidation, microbial mediation | AMP |  1 x 10-3 M [fermentation batches] | 143 |
| Glucose (urate) | (peroxidase and ferrocene) Nafion membrane | electrocatalytic H2O2 reduction | FIA | 200 fmol H2O2, 1.5 pmol Glucose, 2 pmol Urate [serum] | 144 |
| Fructose | (PQQ dehydrogenase, PEI) | nonmediated fructose oxidation | FIA, AMP | 8 x 10-5 M [honey samples] | 145 |
|  | (FDH and Os(bpy)2 complex) | mediated fructose oxidation | FIA, AMP | 4 x 10-5 M [food analysis] | 146 |

Table II  continued

| Carboxylic and Substituted Carboxylic Acids |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Lactate | (Co(II) octaethoxyphtalocyanine, LOd) [paraffin oil] | oxidative H2O2 sensing | AMP | 1 x 10-6 M [sour milks and wines] | 147 |
|  | (Rh, LOd immobil.) | Rh catalysis towards H2O2 or O2 | FIA | 2 x 10-5 M | 148 |
|  | (bienzyme modification, LOd, HRP, PEI) [silicone oil] | H2O2 detection | FIA, AMP | 3 x 10-6 M [fermentation medium] | 149 |
|  | (Co polypyridyl complexes mediators, LADH or LADH + LDH) [mineral oil] | mono- or bienzyme FADH2 and/or NADH oxidation | CV | 5 x 10-6 M [clinical samples] | 150 |
| D-, L-Lactate | (D-lactate dehydrogenase, L-lactate oxidase, HRP, PEI, redox polymer) [silicon or paraffin oil] | mediated NAD(+) reduction, HRP – H2O2 reduction | FIA | 100 (10) x 10-6 M, resp. [fermentation broths] | 151 |
| Ascorbic acid | [diisooctylphtalate] | AA chemisorption on CPE | P | 1 x 10-7 M [NaOH-NaCl medium] | 152 |
|  | CoII-phthalocyanine | catalysed oxidation | DPCSV | 0.8 ppm [fruit juices] | 244 |
|  | (methylene green) | catalytic AA oxidation | FIA | 1 x 10-8 M [model samples] | 153 |
| Ascorbic acid, O2 | (lipid treated CPE) [silicone oil] | O2 reduction, AA oxidation by sequence of pulses | DPV | 10(AA) and 8(O2) x 10-6 M [in vivo measurements] | 154 |
| Oxalic acid | (lead sulfate) | medium exchange, interfacial accumulation | SW ASV | 0.3 mg.L-1 [orange juice] | 155 |
| # Alcohols |  |  |  |  |  |
| EtOH | (ADH, phenothiazine) | electrocatalytic oxidation of NADH | AMP | 5 x 10-6 M [wine] | 156 |
|  | (ADH, HRP, PEI, Os redox gel) [silicone oil] | direct and mediated e- transfer | FIA, AMP |  10-6 M [model samples] | 157 |
| EtOH (Lactate) | PPD and PAP coating (ADH, LOd) | electrocatalytic NADH oxidation | AMP | 8 x 10-10 M | 158 |

Table II  continued

| Glycerol | (GIDH and NAD(+)), PPD polymer | electrocatalytic NADH oxidation, adenine oxidation | AMP | 4 x 10-7 M [plant extract syrup] | 159 |
| --- | --- | --- | --- | --- | --- |
| EtOH, NADH | zirconium phosphate MCPE (Nile blue, NMP mediator, ADH) [paraffin oil] | electrocatalytic NADH oxidation | AMP | 2 x 10-6(NADH) M, ~ 10-4 M (EtOH) [model samples] | 160 |
| NADH (EtOH, Glucose) | (methylene green) [nujol] | electrocatalytic NADH oxidation | CV, FIA, AMP | 1 pmol [model samples] | 161 |
| # Amino Acids, Peptides, Heterocyclic Compounds |  |  |  |  |  |
| Tryptophan | [solid paraffin] | CPE anodic pretreatment, anodic scan | AdSV | 2 ng.mL-1 [injection, synthetic serum] | 162 |
| Uric acid | (uricase, HRP) | enzymatic reduction of H2O2 | FIA, AMP | 3 x 10-6 M [serum] | 163 |
|  | (PVP CPE) [mineral oil] | uric acid catalytic oxidation | SWV | 2 x 10-7 M [human urine] | 164 |
| L-Prolin | (-cyclodextrin) [paraffin oil] | enantioselective membrane construction | CHP | 1 x 10-5 M [biological samples, food] | 77 |
| L-Phenyl-alanine | (salicylate hydroxylase, tyrosinase, L-Phenylalanine dehydrogenase) | enzymatic/electrochemical recycling of tyrosinase | AMP | 5 x 10-6 M [human serum] | 165 |
| S containing amino acids | (crown ethers) | host-guest complex formation | V | 2 x 10-8 M | 166 |
| Cysteine, Glutathione | (Ru(III)-DPDTC) [paraffin oil] | electrocatalytic analytes oxidation | AMP, CV | ~ 3(Cys) and 6(Glu) mg.L-1 [model samples] | 167 |
| Cysteine | Si-NiTsPc MCPE | electrocatalytic Cys oxidation |  |  | 168 |
| [Lys]8]]-vasopressin, Angiotensin II | [mineral oil] | tyrosine residue oxidation | PSA | ~ 10-9 M [model samples] | 169 |

Table II  continued

| Human IgG | (alkaline phosphatase labeled IgG, 3-indoxyl phosphate) | anodic pretreatment, EIA, indigo detection | ACV | ~ 10-10 M | 170 |
| --- | --- | --- | --- | --- | --- |
| Insulin, myoglobin | [mineral oil] | adsorptive accumulation on anodically pretreated CPE | PSA | 2 x 10-9 M [model samples] | 171 |
| Bioactive peptides | [mineral oil] | oxidation of tryptophan and/or tyrosine | PSA | 2 x 10-10 M [model samples] | 172 |
| IgG | (alkaline phosphatase label) | electrochemical EIA | CV, AMP | 2.3 x 10-12 M | 173 |
| # DNA, RNA |  |  |  |  |  |
| tRNA | [mineral oil] | CP anodic pretreatment, adsorptive accumulation | PSA | 4 x 10-16 M [model samples] | 174 |
| DNA | [mineral oil] | guanine oxidation | PSA | 15 ng.mL-1 | 175 |
| DNA, RNA | [mineral oil] | guanine oxidation | PSA | 20 ng.mL-1 [model samples] | 176 |
| DNA (HIV-1) related | oligonucleotide immobil., Co(phen)33+ indicator [mineral oil] | target hybridization | PSA | 4 x 10-9 M [model samples] | 177 |
| DNA, RNA | [mineral oil] | guanine oxidation | FIA, AMP | 460 pg [model samples] | 178 |
| Adenin | [paraffin oil] | oxidative pretreatment of CPE, medium exchange | SWV | 2 x 10-7 M [model samples] | 179 |
| PNA | [mineral oil] | adsorptive preconcentration | PSA | ~ ng.mL-1 [model samples] | 180 |
| DNA | immob. of inosine probe on CPE | detection of duplex formation by appearance of guanine peak | CHP | 120 ng.mL-1 [hybridization sensing] | 181 |
| # Pesticides |  |  |  |  |  |
| Thiram (T) and Disulfiram (D) | Cobalt phtalocyanine mediator | adsorptive accumulation, analyte oxidation | DPV, AdSV | 7 (T) and 2 (D) x 10-8 M [strawberries] | 182 |

Table II  continued

| Ioxynil (I), 2-Me-3-nitro-anilin (M) | (C 18) | electrochemical oxidation | AdSV | 1 (I] and 3 (M) x 10-7 g.mL-1 [drinking water] | 183 |
| --- | --- | --- | --- | --- | --- |
| Matamitron | (silica) | electrochemical reduction | AdSV, SWV | 4 x 10-10 M [soils, natural waters] | 184, 185 |
| Phosalone, Carbophos | (Co(II)2,2´-dipyridylate) | mixed Co(II)-ligand complexes formation | V | 5 and 1 x 10-9 M, resp. [alkaline hydrolyzates] | 186 |
| Karbation et al | (crown ethers) | host-guest complexes formation, electrochemical oxidation | AdSV | 4 x 10-9 M | 187 |
| Phenytoin, Phenobarbital | (Nafion) | ferroceneammonium and cobaltocenium ion redox label determination | SWV | 2 x 10-7 M [dual immunoassay] | 188, 189 |
| Phenolics |  |  |  |  |  |
| Hydroquinone derivatives | [paraffin oil] | analyte oxidation adsorptive preconcentration | DPV | 0.07 mg.L-1 [cosmetics] | 190 |
| Phenols | (tyrosinase) | on line SPE, biosensing | AMP | ~ 1 x 10-6 g.L-1 [river water] | 191 |
|  | (tyrosinase) | biocatalytic accumulation | CHA | 2 x 10-8 M [environmental samples] | 192 |
|  | (HRP, H2O2,lactitol ) [paraffin oil] | phenoxy radicals electrochemical reduction | FIA, AMP |  10-6 M [river water] | 193 |
|  | (solid paraffin) | adsorption on anodically pretreated CPE | ASV | 5 x 10-8 M [tap, waste water] | 194 |
|  | (C10 to C14 , tyrosinase] | extractive accumulation | FIA | 6 x 10-9 M [river water] | 195 |
| Flavonoids | [nujol] | electrochemical oxidation | AdSV | ~ 10-8 M [multivitamin preparations] | 196 |
| Flavanols | (polyphenol oxidase) [nujol] | plant tissue biosensors | AMP | [beers, lagers] | 197 |

Table II  continued

| Flavonoids | [nujol or diphenylether] | direct and medium-exchange determination | AdSV, FIA | ~ 10-8 M [multivitamin preparation] | 198 |
| --- | --- | --- | --- | --- | --- |
| 2-Nitrophenol | (bentonite) | electrochemical reduction | FIA, DPV | - mg.L-1 [sea water] | 199, 200 |
| 2-Methyl-4,6-dinitrophenol | (hidepowder) | reduction of nitro group | CV, DPV | 3.2 x 10-6 M | 201 |
| Salmonella cells | alkaline phosphatase-labeled antibody conjugation [paraffin oil] | EIA, based on measuring phenol oxidation peak | DPV | 5 x 103 cells.mL-1 [models for food analysis] | 202 |
| Catechin and acridine deriv. | (DNA) [pharmaceutical vaseline] | analytes intercalation to DNA | DPV | ~ 10-9 M [model samples] | 203 |
| Catechol-amines | solid CMCPE (tyrosinase) | electrochemical oxidation | HPLC-ECD | 290 pg [model samples] | 245 |
| Dopamine | (potato tissue polyphenol oxidase) | nonmediated biosensing | AMP | 3 x 10-6 M | 204 |
| Dopamine (phenols) | (tyrosinase) [solid paraffin] | quinone sensing | FIA | 5 x 10-8 M [senzor stability study] | 205 |
| Dopamine (uric acid) | [clay] (Nafion) | preanodization, charge-inclusion | SWV | 3 x 10-9 M (2 x 10-7 M) [human urine] | 206 |
| ## Pharmaceuticals |  |  |  |  |  |
| Cephalosporin antibiotics | (fatty acid) | electrochemical analyte oxidation | DC SV | ~ 10-8 M [urine, serum] | 207 |
| Aceclofenac | (hydrophobic substances as fatty acids, surfactants) [nujol] | electrochemical analyte oxidation | AdSV | 2 x 10-8 M [formulations] | 208 |
| Phenylephrine | (cation exchange resin) [paste Metrohm 62801000] | electrochemical analyte oxidation | ASV, LSV | 2 x 10-6 M [urine] | 209 |
| Phenothiazine drugs | (DNA) [mineral oil] | DNA-phenothiazine intercalation | CHP | 5 x 10-9 M [model samples] | 210 |
| Clenbuterol | (Nafion) | electrochemical oxidation | DPV | 1 x 10-9 M [bovine urine] | 211 |

Table II  continued

| Phenytoin | 1-octanol, Nafion loaded CPE | competitive EIA | SWV | 5 x 10-9 M [serum] | 212 |
| --- | --- | --- | --- | --- | --- |
| Doxazosin | bare CPE, Tenax MCPE | electrochemical reduction | AdSV, SWV | 4 x 10-11 M [urine, formulations] | 213 |
|  | (C8) | doxazosin oxidation | DPV, SWV, AdSV | 7.4 x 10-10 M [urine, formulations] | 214 |
| Imipramine | (fatty acid) | electrochemical oxidation | V | 1 x 10-9 M [pharmaceuticals, biol. s.] | 215 |
| Imipramine (I), Trimipramine, Thioridazine | (-cyclodextrine) [pharmaceutical vaseline] | inclusion complexes formation | CV, DPV, AdSV | 7 x 10-9 M Thioridazine 2 x 10-8 M I and Trimipramine [tablets] | 216 |
| Daunomycin | (DNA) | daunomycin-DNA intercalation | CV, PSA | DNA-drug interactions | 217 |
| Nifuroxazide | (polystyren/DVB) | electrochemical NO2 group reduction | AdSV | 10 x 10-9 g.mL-1 [urine] | 218 |
| Aztreonam | (gelatin) |  | DPV, SWV | 8 x 10-8 M [urine] | 219 |
| Indomethacin | [nujol or silicone or castor oil] | electrochemical oxidation, extractive accum., medium exchange | V | 3 x 10-8 M [urine] | 220 |
| Prazosin | (Nafion) | accumulation at 750 mV followed by cathodic sweep | AdSV | 3 x 10-11 M [tablets, urine] | 221 |
|  | (C8) | oxidation of Prazosin | AdSV, DPV, SWv | 8 x 10-10 M [urine, formulations] | 222 |
| Buprenorphine | [paraffin oil] | electrochemical analyte oxidation | CV, DPV, FIA | 1 x 10-8 M [pharmaceuticals, urine] | 223 |
| Azepine, Phenothiazines | [DNA] | drug-DNA intercalation | DPV | ~ 10-9 M | 224 |

Table II  continued

| ## Peroxide Determination for Organic Analysis |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| H2O2 | (asparagus tissue and ferrocene) [mineral oil] | generated ferricinium ion reduction | FIA, AMP | 4 x 10-7 M [milk] | 225 |
|  | (HRP immobil. in silica sol-gel) | hexacyanoferrate(II) mediation | FIA, AMP | 2 x 10-5 M [glucose senzor] | 226 |
| H2O2, 2-BP | (HRP or fungal peroxidase) [paraffin oil, lactitol] | peroxide detection | FIA | 2(H2O2) and 100 x 10-7 M [model samples] | 227 |
| H2O2 | TEMPO loaded CPE [silicon oil] | electrocatalytic oxidation of H2O2 | AMP | 5 x 10-8 M [model samples] | 228 |
|  | (Meldola Blue, fumed silica, HRP) [paraffin oil] | H2O2 bioelectrocatalytic reduction | CV, FIA, AMP | 1 x 10-7 M [glucose, lactate etc] | 229 |
|  | (zucchini peroxidase) | oxidation of guaiacol | FIA, SPFT | 2 x 10-6 M [pharmaceuticals, water] | 230 |
|  | HRP-ferrocene MCPE coated by PAP | H2O2 detection | FIA, AMP | 9 x 10-9 M [milk] | 231 |
|  | (HRP and 3,3´,5,5´-tetramethylbenzidine , GOD) | H2O2 detection | AMP | 10-8 M [Glucose determination] | 232 |
| Other substances |  |  |  |  |  |
| Estrogens | [oleic acid] | analyte electrochemical oxidation | AdSV | 4 x 10-7 M [pharmaceuticals] | 233 |
| Ephedrine | sepiolite | adsorptive preconcentration | SWV | 3 x 10-6 g.L-1 | 234 |
| Cocaine | [paraffin oil] | analyte oxidation | FIA, AMP | 2 x 10-7 M [confiscated goods] | 235 |
| Cholesterol | (hydroxymethyl ferrocene, HRP) | direct determination | CV, CHA | 1 x 10-6 M [serum] | 236 |
| Nicotinic acid | (bacterial Pf cells, p-benzoquinone) | electrocatalytic hydroxylation of nicotinic acid | AMP | 5 x 10-6 M [model samples] | 237 |

Table II  continued

| Surfactants | CPE-ISEs | ion pair formation equilibrium | potentiometric titrations | 1 x 10-5 M | 246 |
| --- | --- | --- | --- | --- | --- |
| Anionic surfactants | (NPOE, ferrocenyl surfactant) | indirectly, from ferrocenyl oxidation wave | AdSV | 1 x 10-7 M [model samples] | 238 |
| Creatinine, Creatine | ferrocene-embedded CPE with entrapped peroxidase | H2O2 determination | AMP | 1 x 10-8 M [serum, urine] | 239 |
| Roxarsone | (Amberlite LA2) [paraffin oil] | analyte reduction, extractive accumulation using cation exchanger | DPV | 1 x 10-7 M [drinks, tablets] | 240 |
| NAD(P)H | (peroxidase and ferrocene MCPE , 1-methoxyphenazine methosulfate) | mediated NAD(P)H oxidation with H2O2 mediated detection | AMP | 4 x 10-8 M [serum, enzyme activity] | 241 |